# Magnetic watering test - examples

- What NDT methods do you know that are based on the magnetic principle?

- Scattering field methods, magnetic structuroscopy methods, eddy current methods

- What physical quantities define a magnetic field?

- Magnetic field strength, magnetic induction, permeability of matter

- What three basic rules apply to the behaviour of induction lines?

- Lines are always closed curves, they do not intersect anywhere, and they go from the south to the north pole

- How do we classify substances according to their magnetic field behaviour?

- Diamagnetic, paramagnetic and ferromagnetic substances

- What is a magnetic domain and how does it relate to the process of magnetization?

- A magnetic domain is a formation to which all atoms with the same magnetic moment fall, according to the size of the domains and the way they rotate; or by determining the behaviour after the magnetization, they determine the suitability of the material to perform the magnetic test

- What is a magnetic hysteresis loop?

- It is a closed magnetization curve, which expresses the dependence of magnetization M on the intensity of the magnetic field H at a slow, smooth change of the intensity of the magnetic field

- What does the magnetization curve describe?

- It describes the dependence of magnetic induction on the intensity of the magnetic field in a given environment

- What is the working range of the magnetic powder method in relation to the intensity of the magnetic field?

- According to the ČSN standard, the intensity value in the given examined material must reach 2-6 kA/m

- Define the term magnetic scattering field.

- Part of the magnetic flux running outside the expected path (in the case of a surface defect, the defect emerges from the magnetized object above its surface into the air); due to the magnetic conductivity of the air, it bridges the defect,

- and, behind the defect, it spreads further through the object

- Briefly describe how the magnetic powder method works.

- If we apply a fine ferromagnetic powder to the magnetized object, it will be caught by the scattering flux over the crack (it will create a kind of "ferromagnetic bridge"). The powder will not be caught in places outside the defect

- What are the possibilities of component magnetization?

- Longitudinal, transverse and combined magnetization; alternating and direct magnetization

- What defects can be detected by the magnetic powder method?

- Surface and subsurface (depending on the type of magnetization from 2 - 10 mm below the surface); defects must also intersect the magnetic field lines at least at an angle of 45°

- Why is it necessary to perform magnetization in two directions?

- To avoid the situation that the defect could be parallel to the direction of magnetization

- What types of magnetic fields do we distinguish?

- Longitudinal and transverse

- What are the advantages and disadvantages of DC and AC magnetization?

- DC magnetization: deep defects can be detected; demagnetization is required; the magnetic field does not "copy" the surface, which increases the probability of false indications

- Alternating  (AC) magnetization: it "copies" the surface of the part well; spontaneous demagnetization occurs; high density of the magnetic field on the surface of the part, which results in a higher sensitivity to small defects

- What is the difference between using a colour suspension and a fluorescent one?

- When using a colour suspension, the defect is detectable based on colour contrast; in the case of a fluorescent suspension, the defect is detectable under UV lamp illumination, when it begins to emit light itself - brightness contrast = more sensitive method

- What are the Hall probe and the Berthold gauge used for?

- The Hall probe is used to quantify magnetic field values (magnetic field strength)

- The Berthold gauge is used to verify whether the magnetization of the object achieves a sufficient value

- Is it possible to use permanent magnets as a source of magnetization for the test?

- Yes