Materials for Lectures and Independent Work

Ing. Petra Čejková, IWE.

2022

- Calculation of carbon equivalent

Formula

Where t = thickness of the material

Cekv is a prerequisite for guaranteed weldability

- Calculation of carbon equivalent

The International Welding Institute has designed the formula in the following form:

Formula

This formula is valid for the following material composition:

(for steel whose carbon content is˃0.18 weight%.)

0.45 for steel sheet thickness lower than 4 mm

0.35.for thickness25 mm

0.3 for 50 mm; suitable, steel can be welded without pre-heating

- Calculation of carbon equivalent

The Czech standard ČSN EN 1011 specifies the relation that is probably the most often used these days

- For the elimination of hydrogen cracking

- Designates the carbon equivalent as CET:

Formula

- Calculation of carbon equivalent

This formula is valid for the following material composition:

Table

- Calculation of the pre-heating temperature

According to Séferian:

Formula

s = thickness of the material

Suitable for carbon and low-alloyed steels where C ˃ 0.1%

- Calculation of the pre-heating temperature

According to It and Bessy:

Formula

H = content of diffuse hydrogen (ml/100g)

K = joint stiffness diffusion coefficient = 69.s for blunt joint (66.s for angle joint)

S = material thickness (mm)

Other calculation relations are set in the Czech standard ČSN EN 1011-1

- Calculation of the cooling time

For three-dimension heat flow

Formula

Where:

T0 = temperature of the sheet while welded

Q = heat input

F3 = weld joint factor

- Calculation of the cooling time

For two-dimensional heat flow

Formula/vzorec

Where:

T0 = temperature of the sheet while welded

Q = heat input

d = sheet thickness

F3 = weld joint factor

- Power properties of electrodes

Aimed at:	- monitoring the weight usage of electrodes

- monitoring the productivity of welding

WELDING POWER

Pn = Gn/t (g/min)

Where Gn = weight of welded metal caterpillar (g)

t = time of surface welding of the welding caterpillar whose weight is Gr (min)

MELTING POWER

Pr = Gr/t (r/min)

Where: Gr = weight of the melt electrode core (g)

t = time of melting the electrode core whose weight is Gr (min)

- Power properties of electrodes

Aimed at:	- monitoring the weight usage of electrodes

- monitoring the productivity of welding

ELECTRODE YIELD

nj = (Gn/Gr).100 (%)

Where: Gn = weight of welded caterpillar metal (g)

Gr = weight of the melt electrode core (g)

MELTING COEFFICIENT

Where: Pr = melting performance/power (g/min)

l = medium permissible welding current (A)

- Amount of energy consumed per …

Can be related to:

- Amount of melt metal Nr

Nr = (U.l.t)/Gr (W.min/g)

- Amount of surface-welded metal Nn

Nn = (U.l.t)/Gn )W.min/g)

Where:  	U = welding arc voltage (v)

l = welding current (A)

t = burning time of the welding arc (min)

Gr = weight of the melt electrode core (g)

Gn = Weight of the surface-welded caterpillar metal (g)

Nr or Nn = specific consumption of power energy (W.min/g)

- Diffusion

Due to basic diffusion equations, the dependence of the diffusion coefficient D on the temperature t has been empirically found:

Formula

Where: D0 is the frequency factor

Q is activation diffusion energy

k is the Boltzmann constant

The depth of the diffusion layer X can be expressed, using the second Fick law, as the dependence of the diffusion coefficient (D) and the time (t)

Formula

𝑥	= 2𝐷. 𝑡𝑑

Where: x if the diffusion depth (cm)

D is the diffusion coefficient (cm2.s-1)

t is the diffusion time (s)

- Coefficient of the weld shape (form)

Picture

Formula	where c = h + a

| Welding method | Ratio b/h |
| --- | --- |
| Electric arc | 2:1 |
| Plasma | 1:1 up to 1:2 |
| Electron beam | 1:5 up to 1:30 |
| Laser | 1:5 up to 1:20 |

- Influence of the welding method

Heat input of electric arc welding

The heat input into the weld bath (Q) is an important parameter, influencing the properties of weld joints (especially in the case of hardly-weldable materials); its size can be calculated using the following relation:

Formula

Where:

ɲ - Efficiency of the welding method (-)

U - Arc voltage(V)

l - Welding current (A)

v Welding speed (mm/s)

- Heat efficiency of individual welding methods

Heat input of electric arc welding

Q = ɲ . (U.l)/1000.v (kJ/mm)

| Method no. | Welding method | k |
| --- | --- | --- |
| 12 | Welding under flux | 1.0 |
| 111 | Manual arc welding with coated electrode | 0.8 |
| 131 | Arc welding with melting electrode in inert gas; MIG welding | 0.8 |
| 135 | Arc welding with melting electrode in active gas; MAG welding | 0.8 |
| 114 | Arc welding with filled electrode without protective gas | 0.8 |
| 136 | Arc welding with electrode filled with flux in active gas | 0.8 |
| 137 | Arc welding with electrode filled with flux in inert gas | 0.8 |
| 141 | Arc welding with tungsten electrode in inert gas | 0.6 |
| 15 | Plasma welding | 0.6 |

- Temperature field

Modified differential equation of heat conduction.

A simplified form of the equation for the temperature of any point in a heat-influenced region can be expressed as follows:

Formula

Where:

T = temperature of the chosen place (°C)

To = initial temperature (°C)

q = heat performance of the welding source (J.A-1)

c = heat capacity (J.g-1°C)

p = specific weight (g.cm-3)

ʎ = heat conductivity coefficient (W.cm-1.s.°C-1)

v = welding rate (cm.s-1)

s = material thickness (cm)

t = time (s)

p/ʎ = α heat conductivity coefficient (cm.s-1)

- Calculation of the characteristic parts of the ARA diagram

Calculation of the temperature of the emergence of martensite

Formula

Calculation of the temperature of the final martensite change

Formula

Calculation of the temperature of the emergence of the bainitic structure

Formula

Heat input

Values in picture/hodnoty v obrázku

Formula/vzorec					Formula/vzorec

Energy amount per length unit

Q1…..Welding input(kJ*mm-1)				Q2…..Welding input(k*cm-1)

I……Welding current (A)					I……Welding current (A)

U…….Welding voltage (V)				U…….Welding voltage (V)

V1…..Welding rate (mm*s-1)				V1…..Welding rate(cm*min-1)

Formula      		Qsv 	Energy loaded into welding joints

Qcel	Total energy of the arc

- Heat input – real

Table

Q3 = Q1,2*ɲ

ɲ … efficiency factor

| Welding technology | Efficiency of the process ɲ |  |  |
| --- | --- | --- | --- |
|  | Extent | Recommended | Resources |
| 111 – MMAW (SMAW) | 0.66-0.85 | 0.8 | (1,3) |

Welding MAG- 135				Formula

Ψ…. Wire diameter  0.8 (mm)

ɲ…Efficiency coefficient 0.7

I     Welding current 110 (A)

U….Welding voltage 20 (V)

v…..Welding speed 2 (mm/s)

f….Joint coefficient = surface weld

Welding MAG-135-pulse			Formula

Ψ…. Wire diameter  0.8 (mm)

ɲ…Efficiency coefficient 0.7

I     Welding current 110 (A)

50%lp, 50%lb (e.g. time of the pulse)

U….Welding voltage 20 (V)

v…..Welding speed 2 (mm/s)

f….Joint coefficient = surface weld

Welding rate

Joint coefficient = surface weld

Formula

MAG-135  Welding

| Welding parameters |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Weld caterpillar | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| Current I (A) | 143 | 204 | 182 | 182 | 208 | 218 | 209 | 203 |
| Voltage U (V) | 16 | 18 | 17,8 | 18,4 | 18,2 | 18,3 | 18 | 18,3 |
| Time (s) | 190 | 185 | 145 | 180 | 190 | 189 | 190 | 185 |
| Speed vs (mm.s-1) | 2.11 | 2.16 | 2,76 | 2,22 | 2,11 | 2,12 | 2,11 | 2,16 |
| Heat input Q (kJ.mm-1) | 2.92 | 1.44 | 1 | 1,28 | 1,53 | 1,61 | 1,54 | 1,26 |

Formula/vzorec			Q - ?  Maximum Q condition

Q =	(Q1 + Q2 ….Q10 )/10			Qmax˂/=Q

Q1, Q2 …. or Q