## Slide 1
ESF II Project of the University of West Bohemia
in Pilsen
Reg No. CZ.02.2.69 / 0.0 / 0.0 / 18_056 / 0013239

## Slide 2
Selected Chapters from Welding
Full-time and Part-time Forms of Study
Ing. Petra Čejková, IWE.
Prerequisites and co-requisites: course TTSS/KMM - 2nd year of bachelor study

## Slide 3: Hybrid welding methods Electric arc welding Orbital welding Plasma welding Laser welding Electric beam welding Welding vs. soldering Weldability Electrical resistance welding
1/52

## Slide 4: 1. Hybrid welding methods
Hybrid welding methods are processes in which two different welding methods are combined in order to achieve optimum weld quality and welding speed.
Energy is supplied to the melting bath by both sources simultaneously.
These methods use the advantages of the two methods used; at the same time, their shortcomings are suppressed, which will be discussed in more detail in the following chapters.
Hybrid welding is mainly used in areas where it is necessary to weld large parts and various types of materials, and where there are high quality requirements.
These include, for example, the automotive, marine, railway, energy and construction industries. The most commonly used combinations include laser + electric arc (MIG, MAG, TIG), plasma + laser, plasma + electric arc, and TIG + MIG.

## Slide 5: Advantages and disadvantages of partial methods
Laser welding
One of the main advantages of laser welding is the small amount of heat input, and thus also small deformations and low internal stresses. Other advantages of laser welding include the possibility of welding a wide range of materials, achieving a high welding speed and productivity, the possibility of welding without additional material, high repeatability and the possibility of local welding even in hard-to-reach places. The disadvantages of laser welding include low gap-bridging, high acquisition costs for relevant equipment, low efficiency and insufficient mobility.
Electric arc welding
The main advantage of this method is high efficiency (up to 80%) and easy bridging of the contact gap. With this method, it is also possible to weld materials with high surface reflectivity. The advantage of MIG/MAG methods is the possibility of welding in all positions and high welding speed. The advantages of the TIG method include the possibility to weld without additional material and the high arc temperature. The disadvantage of electric arc welding is the porosity of the weld metal, which leads to a reduction in toughness, a large TOO and a higher deformation compared to laser welding.
Plasma welding
The advantages of plasma welding include high efficiency, a large ratio of weld depth to width and a high welding speed. Compared to laser welding, this technology also has lower costs. On the other hand, the disadvantage of this technology is a lower performance density compared to the laser.

## Slide 6: Hybrid methods
Laser + electric arc (LaserHybrid)
Principle of the method: During laser welding together with one of the methods of electric arc welding, energy is supplied to the melting bath by both sources simultaneously. First, a laser beam proceeds, which melts the material and forms a welding layer. It is followed by the arc welding equipment at a distance of one to several millimeters. Additional material is supplied and the welding is performed by the classic method of electric arc welding. This procedure is shown in the figure.
Figure 1 - Principle of the laser welding together with electric arc

## Slide 7: Advantages of the LaserHybrid method
Advantages of the LaserHybrid method include large bridging of joints, or even their filling with additional material, low heat input and deep penetration.
The speed of automated welding using this method can be up to 8 meters per minute, while high-quality welds are achieved.
In contrast to separate laser welding, in the case of the production of fillet welds, a deeper weld of higher strength occurs.
The cost-effectiveness of the process is also a benefit. Although the cost of the laser is higher, hybrid welding is faster than the stand-alone MIG method, consumes less gas and reduces the amount of welding consumption of the electrode due to its low heat demand. Thanks to the lower arc and the optimized weld, the consumption of additional material is also significantly reduced.

## Slide 8: Laser + electric arc (LaserHybrid)
By welding butt welds using this method, we also obtain good weld geometry. When welding with a laser, the surface of the weld is recessed; when welding with an electric arc, the weld is very massive. When these methods work together, a weld with minimal cant is created, which is shown in Figure 2. Figure 3 shows a smaller TOO and a more homogeneous weld structure achieved by hybrid welding compared to the MA method.

## Slide 9: Laser + electric arc

## Slide 10: Laser + electric arc
Application of LaserHybrid welding is also suitable for joining various materials, such as aluminium + steel. This method is suitable for applications in conjunction with industrial robots, because the potential of this method can only be used in automated processes. This technology is thus used in the automotive industry (the technology is used, for example, by the VW Group), in the military industry, in electronic production and in the production of medical technology. Other examples of the use of this technology are the welding of aluminium alloys for the production of carriages for rail transport or the joining of ship structures. An interesting application of LaserHybrid is its use in welding materials for the aerospace industry. Here it is used for welding magnesium, aluminium and titanium alloys.

## Slide 11: Plasma + laser (PALW)
This method combines cheaper plasma welding with laser welding. Plasma serves only for preheating, immediately followed by laser welding. Figure 4 shows this method schematically. The angle of inclination of the laser head is 10° backwards from the vertical with respect to the welding direction, in order to prevent potentially destructive back reflections from the surface. It is possible to weld without additional material or with it. The filler material is mainly used for aluminium welding.

## Slide 12: Advantages of PALW
Advantages of the method
The main advantages of the PALW method are:
high performance (up to one-third higher than when using a stand-alone laser)
greater weld width and high welding speed while maintaining deep penetration and the quality and accuracy of the weld
the efficiency of the process is high, compared to separate laser and plasma welding
slower cooling of the welded part, and therefore less increase in the hardness of the weld metal
This method also has advantages when welding thin sheets.
Compared to the use of a separate laser; the welding speed can be increased by up to 50% and, at the same time, a high-quality weld with minimal defects is created.
Financial advantage: relatively expensive laser power is partially (up to 50%) replaced by cheaper plasma power.
It is possible to replace additional wires with powder that is more usable, or to omit additional material completely.

## Slide 13: Comparison of the appearance of resulting welds
Plasma
Laser
Plasma and laser
The figure shows a comparison of the weld cross-sections and the deep penetration when using the PALW method.

## Slide 14: Use
The laser welding method together with plasma can be used for a wide range of materials, such as steel and aluminium. Applications of the PALW method include the automotive industry; for example, it is used for welding fillet welds connecting cast parts and extruded profiles to the Audi A8. It is also often used in the production of custom semi-finished products, due to the large number of usable materials, the possibility of deep penetration and affordability.

## Slide 15: Plasma + MIG
1/52
The principle of the Hybrid Plasma Welding method together with MIG (PMHW) uses two separate sources of welding current. The welding process can be defined as a combination of plasma arc welding and MIG welding within a single torch, where an additional wire is fed through the plasma nozzle orifice. The PMHW arc consists of a MIG arc (inner arc) surrounded by a plasma arc (outer arc). [9] The plasma arc also surrounds the MIG wire and the weld bath, thereby preheating and reheating the wire and the parent metal [1]. The arrangement of the welding system is shown in the figure
PMHW welding method scheme

## Slide 16: Advantages of the method
The PMHW method is characterized by high deposition rate, high efficiency and excellent wettability. It is preferably used for welding copper. Copper welding by a separate MIG method is problematic due to lower arc stability and high thermal conductivity. In addition, welding heterogeneous welds (such as from copper to carbon steel) is more difficult due to the difference in thermal conductivity. The plasma arc effectively preheats the material and also has a positive effect on the stability of the MIG arc. The resulting appearance of the weld can be seen in Figure 7, where you can see greater weld depth and more uniform caterpillars/beads using the PMHW method. This method is also used in aluminium welding. The resulting weld shows low porosity; moreover, the plasma arc physically cleans the oxide film on the aluminium surface. A wider use of this method is prevented by its high cost, as it is necessary to use two separate sources of welding current.

## Slide 17: Comparison of weld depth and caterpillars PLASMA + TIG

## Slide 18: TIG + MIG: the principle of the method
TIG + MIG hybrid welding has two variants: TIG-MIG and MIG-TIG, determined by the position of the electrode (relative position between the wire and the tungsten electrode with respect to the welding direction). When the leading arc is a TIG followed by a MIG, welding is referred to as hybrid TIG-MIG welding, while the welding process with the reverse order of the arcs is referred to as MIG-TIG. This difference is shown in the figure. If the TIG arc is conducting, the TIG current should be higher than the MIG current to ensure arc stability. The leading TIG arc is more effective in improving arc stability, while the case where the TIG follows the MIG is more suitable for suppressing defect undercutting.

## Slide 19: Advantages of the TIG method
It stabilizes the arc and increases the depth of penetration. This method thus combines the high quality of the TIG process together with the high efficiency of the MIG method. Compared to the conventional TIG process, the hybrid process has a shorter welding time by 17-44%, confirming a significant efficiency improvement. The weld also has a better appearance; there is no oxidation on the surface of the caterpillars.

## Slide 20: MIG + TIG
Comparison of MIG and TIG-MIG welding
a - appearance of the caterpillars
b - cross-section
c - high-speed camera shot
d - current-voltage characteristic of MIG

## Slide 21: Recommended and used literature:
J. TEPLÝ, ANALÝZA SVAŘOVÁNÍ LASERHYBRIDEM, VYSOKÉ UČENÍ TECHNICKÉ V BRNĚ : FAKULTA STROJNÍHO INŽENÝRSTVÍ ÚSTAV STROJÍRENSKÉ TECHNOLOGIE, 2010.
„Svařování - metodou MIG, MAG, TIG,“ KOVORAKO, s.r.o., [Online]. Available: http://www.kovorako.cz/6119/svarovani-metodou-mig-mag-tig/. [Přístup získán 17. 10. 2021].
Page. C.J. et al., „Plasma augmented laser welding and its applications,“ Science and Technology of Welding and Joining , No. 1, Vol. 7, 2002.
Korzhyk, Volodymyr & Bushma, Oleksandr & Khaskin, Vladyslav & Chunlin, Dong & Sydorets, Volodymyr. (2017). Analysis of the Current State of the Processes of Hybrid Laser-Plasma Welding. 10.2991/icmmse-17.2017.14
Hee-Keun Lee, Kwang-San Chun, Sang-Hyeon Park, Chung-Yun Kang, Control of surface defects on plasma-MIG hybrid welds in cryogenic aluminum alloys, International Journal of Naval Architecture and Ocean Engineering, Volume 7, Issue 4, 2015, pp 770-783, ISSN 2092-6782, https://doi.org/10.1515/ijnaoe-2015-0054.

## Slide 22: Thank you for your attention.

## Slide 23: 2. Electric arc welding in protective atmospheres MIG, MAG, TIG

## Slide 24: Welding bath protection
One of the main problems with welding is that metals react faster with the surrounding air atmosphere as their temperature rises.
The method of protecting hot metal from atmospheric attack is the second most important distinguishing feature.
Method of protection:
Fluxes, electrode covers
Protective atmospheres
Special (vacuum, ceramic rings, etc.)
When welding in protective atmospheres, the protective gas is not generated when the arc burns, but is supplied under low pressure from a reservoir (steel cylinder or central distribution) so that the gas constantly flows around the electrode and overlaps and protects the molten welds and molten bath from surrounding atmosphere.

## Slide 25: The role of protective atmospheres
Protection of the weld melt, electrode, arc and weld area
Weld root protection
Influencing processes during ignition and burning of an electric arc (creation of a sufficiently ionized environment)
Maintaining the stability of the arc burning and supporting the transfer of weld metal (influencing metallurgical processes during the formation of a drop of liquid metal at the end of the melting electrode)
Contributing to the transfer of thermal energy to the weld

## Slide 26: The role of protective atmospheres
Protective atmospheres also have an effect on:
Flowability and wettability of the weld melt bath
Weld metal properties
Desoldering power
The shape and dimensions of the weld bead and the size of the penetration
Spray volume and welding speed

## Slide 27: Electric arc welding methods in protective atmospheres
MAG (Metal active gas)
a melting electrode, where the shielding gas actively participates in the formation of the weld metal
MIG (Metal inert gas)
a melting electrode where the shielding gas does not react to form a weld metal
TIG (Tungsten inert gas)
Tungsten non-melting electrode, where the shielding gas does not react during the formation of the weld metal

## Slide 28: MIG/MAG METHOD WELDING
Fusion arc welding with a molten metal electrode, where the electric arc and the weld area are protected from the surrounding atmosphere by a layer of shielding gas supplied from an external source.

## Slide 29: METHOD MARKING according to the Czech standard ČSN EN ISO 4063
131 - Metal inert gas (MIG) melting electrode arc welding - EN
135 - Arc welding with a melting electrode in active gas
(MAG - Metal active gas) - EN
GMAW - Gas Metal Arc Welding
ASM (applies to both MIG and MAG)
FCAW - Flux Cored Arc Welding - filled electrode welding

## Slide 30: MAG (135)/MIG (131) welding principle

## Slide 31: Cut through the end of the torch
1- Welding torch
2- Protective insert
3- Nozzle for supply of shielding gas
4- Contact tip ensuring power supply
5- Welding wire (electrode)

## Slide 32: WELDING BURNER

## Slide 33: CARBON DIOXIDE– CO2
is a strongly oxidizing gas - it is one of the so-called active gases
Characteristics:
Non-flammable, non-toxic and colorless gas, specific acid flavours, boiling point -78.5ºC.
In the solid state, it is white and hard (used for the production of dry ice, e.g. for blasting).
It evaporates rapidly at room temperature and evolves CO2 gas.
Not toxic, but at higher concentrations in the air it prevents breathing (15%).
Production:
Usually based on separation and cleaning of CO2 from industrial and natural sources

## Slide 34: CARBON DIOXIDE– CO2
It can be liquefied by pressure (e.g. at 0ºC at a pressure of 3.6 MPa).
Up to a temperature of 700ºC, CO2 is stable and behaves like an inert gas (chemically inert).
However, at higher temperatures it decomposes into carbon monoxide (CO) and oxygen (O), so it has an oxidizing effect.
(it can be said that 10% CO2 then has the same effect as about 1% O2 ).
For welding, CO2 with a purity of min. 99.5% is used. The rest consists of impurities and moisture, which must not exceed 0.04%.
In cylinders (usually 20 and 40 l), the gas is stored in a liquid state under a pressure of 5 MPa.
(Liter of liquid gas, at 0ºC - gives about 504.5 l of gas).

## Slide 35: CARBON DIOXIDE– CO2
CO2 is removed from the bottle by means of a single-stage reduction valve, while liquid CO2 changes state and turns into a gaseous state.
During the evaporation and expansion of the gas, heat is removed from the environment, which can cause a decrease in temperature during intensive consumption, which leads to possible freezing of the valves.
Therefore, anti-freeze valves are used as CO2 components for CO2 reduction valves and are connected to a welding current source.
The great advantage of CO2 as a shielding gas is, above all, its low price.

## Slide 36: CARBON DIOXIDE– CO2
Properties:
It ionizes worse - (despite a low ionization potential of 14.4 eV)
= higher voltage required
It conducts heat well -
= high heat transfer to the weld bath + the heat obtained by exothermic oxidation reactions ensures very good melting of the weld edges, deep penetration with an oval weld bead profile and good degassing of the weld bath
Heavier than air - (about 1.5 times; specific weight is 1.976 kg/m3)
= good bath protection (especially in common PA, PB, PC positions)

## Slide 37: Metallurgic reactions
Reaction of gas with electric arc:
CO2 → CO + O
Melting bath reaction:
Fe+O → FeO + Q (released heat) C+FeO → Fe+CO (porosity)
Alloying Mn, Si
FeO + Mn = MnO + Fe 2FeO + Si = SiO2 + 2Fe

## Slide 38: Metallurgic reactions

## Slide 39: Influence of correct choice of PM and shielding gas
100% CO2 wire G3Si1
82% Ar+18% CO2 wire G3Si1
Non-alloy steel

## Slide 40: MIXED GASES
One-component shielding gases do not guarantee the required stable welding process and regular metal transfer in the welding of some metals and alloys.
Therefore, they are often replaced by argon-based gas mixtures today.
In order to increase the stability of the arc, gases with an oxidizing effect (active – CO2, O2), or helium are added to argon in order to increase the thermal output.
Advantages of using mixed gases
  Increasing the stability of the welding process
  Reduction of liquid metal spatter
  Improving the formation of the weld bead
  Increasing welding productivity

## Slide 41: Ingredients of mixed and formation gases
OXYGEN – O2
Oxidizing gas
Used only as an additive; has a strong oxidizing effect (higher than CO2)
It weakly ionizes
It conducts heat well
Higher bath temperature; reduces the surface tension of the welding bath; improves the transition to the base material
Higher susceptibility to defects when increasing its content in the mixture (max. 5 %)

## Slide 42: Ingredients of mixed and formation gases
NITROGEN – N2
Unresponsive gas
Carrier gas of moulding mixtures, or special purpose additive (e.g.
duplex)
Risk of nitride formation
Slightly lighter than air
HYDROGEN – H2
Reducing gas
Used only as an admixture (in mixed and formation gases)
It conducts heat well - higher bath temperature, wider weld, higher welding speed
Risk of hydrogen cracking in sensitive materials (max. content up to 10%)
Lighter than air

## Slide 43: Properties of individual components
Ionization and dissociation energies
Dissociation of carbon dioxide (CO2) depending on the temperature

## Slide 44: Properties of individual components
Heat output of the arc
- increases with increasing arc voltage
(Additives of helium and hydrogen in argon mixtures significantly increase the stress on the arc and thus its heat output)
The protective atmosphere used has a great influence on the shape and size of the weld bead

## Slide 45: ADVANTAGES OF MIG/MAG WELDING
Uncovered welding wire can be wound on spools and continuously supplied to the welding bath without frequent and inconvenient replacement of welding electrodes (semi-automatic welding method).
The welding current can be supplied to the wire up to its close melting end using friction contacts (torch contact tips).
As the current-loaded part of the wire is short and uncovered, it is possible to achieve a much higher current density per 1 mm2 of the wire cross section.
Possibility to use a large range of welding parameters for one thickness of welding wire (electrode).
The mechanization of the welding process is greatly simplified, because there is no covering of additional material, which prevents manipulation, and also due to the method of ignition of the electric arc.

## Slide 46: Examples of welded joints

## Slide 47: Automatization and robotization

## Slide 48: MIG soldering
Overlapped joints
Thickness up to 3 mm
Impulse curre (with low base current)
Short arc
CuSi3 –OK Autrod 19.30 Argon, CRONIGON 2 and S1 (Ar + CO2, O2)
CuAl 8 – OK Autrod 19.40
Argon (Ar+He)

## Slide 49: Welding with a filled electrode with its own protection
T his is welding with filled (tubular) wire, but without the use of shielding gas.
According to the ČSN EN ISO 4063 standard, this method is referred to as method:
No. 114 or often also an abbreviation
MOG (metal ohne gas).
FCAW (Flux Cored Arc Welding), but e.g. LE calls it, for commercial purposes, Innerschield
+
136 - Filled electrode arc welding in active gas (MAG, FCAW)
138 - Filled electrode arc welding with metal powder in active gas

## Slide 50: Welding with a tubular electrode with its own protection

## Slide 51: MOG welding
The welding process combines the principles of MMA (coated electrode) welding and MIG/MAG methods.
For the MMA method, it is operability, mobility and resistance to weather conditions + protection of the weld bath using the resulting gases and slag from the electrode shells.
On the MIG/MAG side, high labour productivity due to high desoldering power, it provides easy welding mechanization with continuous wire feeding to the weld site.

## Slide 52: Types of filled electrode fillings

## Slide 53: Types of fillings
Basic – the weld metal is covered with a layer of slag, which contains limestone, fluorides and oxides of aluminium and alkaline earths. Basic fillings have good refining effects on the weld metal, which has a positive effect on notched toughness and resistance to cracks at low temperatures. Slag is harder to remove.
Rutile – the weld metal is covered with a layer of slag, which contains mainly titanium dioxide. This slag is so-called fast-setting and is intended mainly for welding in positions where it helps to form a weld, and significantly increases the welding speed in these positions. The slag is easy to remove.
Metal – the weld metal is without slag; the tube is filled with metal powder, alloying additives and elements stabilizing the burning of the arc. This type has a high yield; the resulting weld is free of slag and spatter. Modern types of these tubes are designed for all welding positions.

## Slide 54: TIG WELDING - PRINCIPLE - METHODS

## Slide 55: TIG, WIG WELDING PRINCIPLE (141)
jeho podávání dle postupu svařování.

## Slide 56: Grinding of tungsten electrodes

## Slide 57: ADDITIVE MATERIALS - solid wires, tubes

## Slide 58: ARGON - Ar
Properties:
It ionizes well - (low ionization potential 15.8 eV)
= possibility of high current load; it ignites the electric arc well;
higher radiation intensity of the arc
It conducts heat worse - (low thermal conductivity)
= wide weld on the surface, narrow weld at the root
Heavier than air - (approx. 1.4 times; specific weight is 1.784 kg/m3)
= good weld bath protection (especially in the PA position)
- low sensitivity to airflow
It forms the basis of mixed gases for welding

## Slide 59: HELIUM - He
FSW – Friction stir welding
is inert - does not form a chemical compound with any element
Characteristics:
monoatomic inert gas, colourless and odourless
Production:
It is produced by separation from some types of natural gas, where He occurs in an amount of about 1%. Helium is present in very small amounts in the air.
Helium is produced in high purity (min. 4.6) with a limited content of impurities (oxygen, nitrogen and water vapour from 5 to 20 ppm).
For welding purposes, helium is supplied in gaseous cylinders, similar to argon (filling pressure 20 MPa).
He

## Slide 60: HELIUM - He
FSW – Friction stir welding
Properties:
It ionizes less - (higher ionization potential 24.6 eV) = worse arc ignition, higher arc voltage required; arc is unstable at longer length
It conducts heat well - (high thermal conductivity) = higher bath temperature, wider weld, higher welding speed, better bath degassing
Lighter than air - (approx. 7 times lighter than air and approx. 10 times lighter than argon; specific weight is 0.178 kg/m3) = reduces gas protection efficiency; larger gas flow required
It is not used to such an extent as a separate gas for manual and semi-automatic welding processes, but rather in mixtures with argon

## Slide 61: BENEFITS OF TIG (WIG) WELDING
FSW – Friction stir welding
Regular formation of the root and the weld surface, high integrity, favourable mechanical and physical-chemical properties of the created joints
There is no oxidation and burning of elements in the metal, so we achieve the same chemical composition of the weld metal as the base material
The weld bath is perfectly protected by shielding gas from the effects of the surrounding atmosphere; welded joints are stronger, tougher and more corrosion-resistant than welded joints welded in most other ways
The weld bath is well visible and relatively easy to handle
It can be welded in all positions; the surface of the welding bead does not need further machining
Easy automation, mechanization and robotization of the welding process
Disadvantage: -lower productivity (usually manual welding)

## Slide 62: Parts of an electric arc
FSW – Friction stir welding

## Slide 63: Arc voltage drop
FSW – Friction stir welding
-
+
Anodová oblast
Katodová oblast
Sloupec oblouku
Elektroda
(katoda)
Základní materiál (anoda)
Zdroj proudu

## Slide 64: Influence of polarity on heat distribution

## Slide 65: "Hot wire" TIG welding
The supplied additional welding wire is preheated by resistance heat when a current supplied by a special source passes.
up to 4times higher welding power
lower risk of pores in the weld
less risk of cold joints
better transfer of alloying elements to the weld (melting wire does not pass through the arc)
minimal cooling of the melting bath by adding additional material,
higher welding speed
reduction of thermal influence of the base material

## Slide 66: Narrow bevel TIG welding
FSW – Friction stir welding
Also called NARROW GAP WELDING
Narrow gap welding is basically multi-layer welding with a specific weld bevel, the shape of which is chosen so that each layer is composed of a maximum of two beads.
With the exception of the root part and the cover layer, all weld beads are usually laid over the entire weld thickness at the same welding parameters.
The construction of the welding nozzle is also very important; it must ensure good guidance of the welding wire near the weld edge, and must have a small thickness due to the narrow gap..

## Slide 67
FSW – Friction stir welding
Thank you for your attention.

## Slide 68: 3.. Orbital electric arc welding
This is a specialized area of welding, which is mainly used for pipe-to-pipe welding. Orbital welding is used mainly in the chemical, pharmaceutical, aerospace, energy (oil and gas pipelines), nuclear and food industries, where high demands are placed on the quality of welds. The advantages include, above all, a perfect penetration of the weld, the creation of a quality weld root and the creation of a visually aesthetic caterpillar. However, it is very difficult to achieve high weld qualities at different welding positions. These are mainly PE (horizontal and overhead) and PD (horizontal and oblique overhead) positions. Due to the problem with non-constant quality of welded joints, manual welding began to be gradually replaced by automated orbital welding.

## Slide 69: History of orbital welding
Orbital welding was developed in the 1960s by Northrop Aircraft Inc. for the needs of the aerospace industry. The research and development was led by Vladimir H. Pavlecka (a Czech native from Roudnice nad Labem); his collaborator was Russ Meredith. This pipe-to-pipe welding system has been used primarily to produce high-strength components such as hydraulic systems. It also caught on very quickly in the nuclear industry. Originally, a specially modified TIG burner was used, which was placed on an orbital carrier. The carrier moved along a special toothed ridge. This method is still used today in modern open welding heads.

## Slide 70: Principle of orbital welding
Orbital welding is automatic pipe-to-pipe welding controlled by a computer. The orbit head is fastened to the outside of the welded pipe using collets. Subsequently, the orbital head performs a circular motion around the axis of the welded pipe and creates a weld. The circular motion is in the range of 365°-375° to guarantee penetration of the beginning and the end of the weld.

## Slide 71: Types of welding technologies for orbital welding
Various welding methods can be used for orbital welding. This is most often the TIG/TIG method. The MIG/MAG method and laser welding are also used. Welding is possible with or without additional material. Using orbital welding, it is possible to weld a large number of metals: the hardest ones, heat- and corrosion-resistant steels, unalloyed and low-alloyed carbon steels, and nickel alloys, as well as titanium, copper, aluminium and all their alloys. Thin-walled and thick-walled pipes can be welded, depending on the welding head used.

## Slide 72: Orbital welding system
The system of each orbital welding consists of the following main parts:
• power supply and regulator
• control computer
• welding head with clamping device
• wire feeding mechanism, if applicable
The quality of the weld is affected by:
arc length
magnitude and pulse frequency of the welding current
welding speed
shielding gas
base material and additional material (if used)
dimensions of welded pipes
preparation of contact surfaces
knowledge and experience of the welder/operator

## Slide 73: Advantages of the method
fast and accurate method
constant arc length
constant feed rate
precise guidance of the welding nozzle
small deformations and small TOO
repeatability - higher productivity in series production
weld aesthetics
no need for manually skilled welders
one welder/operator can operate multiple welders simultaneously

## Slide 74: Disadvantages of the method
high acquisition costs
maintenance required
complexity of the device
need for precisely machined contact surfaces
need for qualified welder/operator

## Slide 75: Welding heads
The most important part of orbital welding are the welding heads. Currently, two basic orbital welding methods are used to produce pipe-to-pipe welds. The first is an open welding head, and the second is a closed welding head. There is also a special type of welding head for the production of pipe-to-pipe welds.
Closed welding heads
Their construction consists of a closed welding chamber in which there is an inert atmosphere. During welding, the electrode rotates 360° around the axis of the welded pipes. The movement is ensured by an electric motor and a system of gears inside the body of the welding head. The head is clamped to the outer diameters of the welded pipes before welding. To prevent overheating, ducts are located inside the head through which the coolant flows. Welded pipe diameters typically range from 3 mm to 170 mm. However, it is necessary to have clamping cassettes of a specific diameter supplied by the manufacturer. This welding method is mainly used for welding thin-walled stainless steel pipes. The TIG/WIG method is most often used for this.

## Slide 76: Open welding heads
Their construction is simpler than in the case of closed welding heads. It consists of eccentric collets that can be easily, precisely and firmly clamped to the outer diameter of the welded pipe. A movable support is attached to the clamps, which uses an electric motor to perform a rotary movement around the axis of the welded pipe. A welding head with a wire feeder is attached to the support. The head must also be cooled to prevent overheating. This method is suitable for welding pipes of large diameters (generally over 170 mm) and larger wall thicknesses. Various methods can be used for this welding method, most often TIG/WIG; MIG/MAG is also suitable for laser welding. In modern welding systems, the electrode has 4 degrees. This is necessary when trying to produce the best possible weld for thick pipes. A powerful computer and a ready-made programme are required for precise control of all movements.

## Slide 77: Closed orbital welding head
closed orbital welding head with power source and control PC; different diameters of closed orbital welding heads

## Slide 78: Open welding heads

## Slide 79: Thank you for your attention.

## Slide 80: PLASMA WELDING

## Slide 81: ELECTRIC ARC
Definition
An electric arc (usable for welding) is a low-voltage high-pressure electric discharge, which usually occurs between the electrode and the base material in an ionized gas environment.
It burns stably provided the voltage is sufficient to ionize the medium and the current keeps the plasma in the arc in an ionized state.

## Slide 82: Plasma
= physical concept introduced in 1923 (I. Langmuir) for a special state of gases, sometimes referred to as the fourth state of matter.

## Slide 83: Plasma
Definition:
Plasma is a quasi-neutral gas of charged and neutral particles, which shows collective behaviour
Thermodynamic processes:
DISSOCIATION
Dissociation is an event in which molecules that are diatomic (e.g., 02, H2, N2) or even more complex (e.g. CO2 ), break down into individual atoms at normal temperature.

## Slide 84: Plasma
By adding energy (mechanical or thermal) to the gases, these are ionized.
IONIZATION is the release of electrons from the valence orbits of atoms. The released electrons have a negative charge and conduct an electric current; ionized nuclei of atoms, ions, with the remaining electrons have a positive charge.
Ionized gas – plasma is therefore electrically conductive, but behaves electrically neutral.

## Slide 85: Plasma
Plasma is the 4th state of matter.
It is basically a concentrated (narrowed) electric arc, which is composed of electrons, ions and neutral particles. These particles in the plasma arc have different charges. As a whole, the steady state plasma is electrically neutral.
Properties:
Large heat capacity
Subject to the effects of electric and magnetic fields
… and mechanical effects
It can be partially or completely ionized:
Partially ionized: 5,000 ÷ 15,000 K
Fully ionized: up to 100,000 K

## Slide 86: Electric arc plasma
Plasma
Is a form of dissociated and highly ionized gas, which allows, due to its properties, the electric arc to burn.
When plasma is generated and maintained by the supply of electrical energy, the resulting plasma formation is called an electric discharge or electric plasma.
In an electric discharge, plasma serves to create a conductive path in an environment that was not originally conductive.
The plasma "during welding" is generated in the plasma burner by the passage of gas through a stabilized electric arc.

## Slide 87: Plasma welding
Plasma welding – designation:
According to ČSN EN ISO 4063:
Method 15
PAW
Plasma Arc Welding
Plasma welding is one of the modern, highly productive methods of arc welding in a protective atmosphere.
It is characterized by very high energy concentration and high operating temperature.

## Slide 88: Electric arc plasma
FSW – Friction stir welding
Plasma welding uses the concentration of heat and the dynamic effect of the plasma, which is the result of the narrowing (focusing) of the electric arc that arises between the tungsten electrode and the weldment.
Electric arc stabilization
A stabilized arc is a concentrated (narrowed) electric arc used in technical practice. It is achieved thanks to:
plasma burner nozzle shape,
flowing gas,
water.

## Slide 89: Electric arc plasma
Plasma gas, which flows around the electrode, expands sharply due to the heat of the arc, and flows through the orifice in the nozzle at a very high speed (Ar).
Secondary (protective) gas is used for self-protection of the melting bath (Ar, Ar + H2).
Gas consumption:
Plasma gas: 0.5-7 l.min-1
Focusing gas: 3-
Protective gas:
3-12 l.min-1
2-16 l.min-1

## Slide 90: Types of gases used

## Slide 91: Types of gases used

## Slide 92: Types of gases used

## Slide 93: Types of protective gases used
FSW – Friction stir welding

## Slide 94: Plasma welding – principle of the method
FSW – Friction stir welding
Plasma welding evolved from the TIG method
- the arc burns between the non-melting electrode and the base material most often in a protective atmosphere of inert gas.
PAW
TIG

## Slide 95: Comparison of TIG and plasma welding
FSW – Friction stir welding
TIG
PAW
1-burner body, 2-centred tungsten electrode, 3-ceramic protective nozzle,
4-narrowed nozzle, 5-protective gas,
6-concentrated plasma arc, 7-electric arc, 8-plasma arc (column)

## Slide 96: Plasma welding - temperature distribution
FSW – Friction stir welding

## Slide 97: Plasma arc temperatures
FSW – Friction stir welding
The plasma temperature will largely depend on what gases are brought into the plasma state.
Individual gases have different physical properties, including ionization potentials; the concentrated electric arc has the following temperatures with respect to the gas used:
Hydrogen
Nitrogen
Argon
Helium
-up to 8,000 K
-7,000 K
-15,000 K
20,000 K

## Slide 98: Plasma welding - weld cross-section
FSW – Friction stir welding
Concentrated heat guarantees deep melting of the base material,
good root formation and a characteristic weld cross-section.
It is a highly stable welding process; it has a characteristic weld formation (the penetration is in the shape of a wine glass), especially the root, which allows welding without root support up to thicknesses of about 10 mm.

## Slide 99: Comparison of TIG and plasma welding
FSW – Friction stir welding
Higher arc temperature
Higher welding speed
TOO (keyhole welding) reduction
Minimal deformation (low heat load)
Very good welds
Weld preparation costs are eliminated
(butt weld without bevel up to t = 10 mm)
By using PM it is possible to bridge gaps (achieve the required cant) - lower PM consumption
High electrode life (pilot arc)

## Slide 100: Plasma welding scheme
FSW – Friction stir welding

## Slide 101: Plasma welding - principle of the method
FSW – Friction stir welding
Unlike TIG welding, a burner with an intensively cooled outlet nozzle of smaller diameter and a nozzle is used, which narrows the arc to a relatively small area of the weldment, i.e. electric arc focusing.
Shielding gas (Ar or Ar + H2) also contributes to the increase in energy density.
A small diameter nozzle burner is used to narrow the arc.

## Slide 102: Plasma welding - manual burner
FSW – Friction stir welding
1 - Electrode cover,
2 - O-ring,
3 Collet,
4 Collet case,
5 O-ring,
6 Spring,
7 Electrode line
8 Electrode,
9 Burner body
10 Centering ceramic tube,
11 Nozzle,
12 Ceramic protective nozzle,
13 Adjustment tool

## Slide 103: Methods of plasma welding
FSW – Friction stir welding
Microplasma welding with a welding current of 0.1-20 A.
(material thickness from 0.01 mm) MICRO
2. Medium plasma welding with a welding current of 20-100 A. (material thickness from 0.6 to 3 mm) SOFT
3. Keyhole welding, above 100 A, where the plasma arc penetrates the wall and, when the welding tube is moved, molten metal is cast at the location behind the "keyhole" due to surface tension.(material thickness from 3 to 10 mm)
4. Plasma soldering
use for soldering galvanized sheets

## Slide 104: Microplasma welding
FSW – Friction stir welding
The arc is stable from 0.05 A (intensity up to 25 A)
It is not possible to immerse the electrode in the melting bath
Material thickness from 0.01 mm to approx. 2 mm
Application: medical technology, measuring instruments; an electric pilot arc ensures reliable ignition of the main arc;
electrotechnics, aircraft technology, aerospace industry, chemical and food industries, etc.

## Slide 105: Keyhole welding
FSW – Friction stir welding
The pilot arc ensures reliable ignition of the main arc
High weld quality and excellent appearance
Material thickness from 3 to 10 mm
High energy density on the surface causes a narrower melting bath and TOO (water-cooled burners are needed)
Thicknesses up to 10 mm (CrNi) can be welded with a single layer weld without demanding preparation of weld surfaces (with good root penetration)
Plasma gas volume (from 0.6 to 10 l/min)
Application: distribution and distribution systems of liquids, tanks and their accessories (CrNi)

## Slide 106: Continuous beam welding - keyholing
FSW – Friction stir welding

## Slide 107: Welding parameters
FSW – Friction stir welding
Basic welding parameters:
Welding current (welding voltage) - affects weld properties through plasma outlet pressure and temperature
Plasma gas flow rate - it is related to the kinetic energy of the arc and therefore also to the depth of penetration
Welding speed
The range should not exceed 20 to 30 cm/min - constant
Composition of plasma and shielding gases (+ flows) - constant
Welding wire feed speed
Burner setting and tungsten electrode type (nozzle diameter, burner distance)
Preparation of basic material

## Slide 108: Advantages of plasma welding
FSW – Friction stir welding
higher welding speed and the possibility of mechanization
smaller heat-affected area, and thus less deformation
smaller overhang of the weld, and thus a reduction in the laboriousness of the subsequent machining of the weld
maintaining favourable mechanical values of the base material
excellent weld appearance with easy reproducibility
excellent weld quality (high purity without pores and bubbles)
very good penetration and weld shape
reduction of laborious preparation of welded surfaces
it is not necessary to bevel the welded surfaces up to a thickness of 8 mm
can be welded in one pass and only on one side,
saving additional material

## Slide 109: Areas of application of plasma welding
FSW – Friction stir welding
high quality and productivity of the process with minimal heat-influencing of the base material
nuclear industry
chemical industry
food industry
electronics
shipbuilding
aviation industry
automotive

## Slide 110: Methods of plasma burner connection
FSW – Friction stir welding
The plasma arc can burn in a transmitted (dependent) or non-transmitted (independent) manner
Dependent connection: for electrically conductive materials
Independent connection: for electrically non-conductive materials

## Slide 111: Types of plasma arcs
FSW – Friction stir welding
A, B) independent (non-transmitted) plasma arc A = blown arc
C) dependent (transmitted) plasma arc

## Slide 112: Plasma welding scheme
FSW – Friction stir welding

## Slide 113: Methods of plasma welding
FSW – Friction stir welding
Microplasma welding with a welding current of 0.1- 20 A.
(material thickness from 0.01 mm) MICRO
2. Medium plasma welding with a welding current of 20-100 A. (material thickness from 0.6-3 mm) SOFT
3. Keyhole welding, above 100 A, where the plasma arc penetrates the wall and, when the welding tube is moved, molten metal is cast at the location behind the "keyhole" due to surface tension.
(material thickness from 3 to 10 mm)
4. Plasma soldering
use for soldering galvanized sheets

## Slide 114: Microplasma welding
FSW – Friction stir welding
The pilot arc ensures reliable ignition of the main arc
The arc is stable from 0.05 A (intensity up to 25 A)
It is not possible to immerse the electrode in the melting bath
Material thickness from 0.01 mm to approx. 2 mm
Application: medical technology, measuring instruments, electrical engineering, aeronautics, space industry, chemical and food industries, etc.

## Slide 115: Clamping of components during microplasma welding
FSW – Friction stir welding
1- clamping elements, 2- attachment, 3- welded material,
4- Cu attachment, 5- groove for shielding gas supply, 6- base plate

## Slide 116: Microplasma arc welding scheme
FSW – Friction stir welding
Microplasma (pulse and continuous) welding is used
mainly for welding thin sheets
1- non-transmitted arc source, 2 - ionizer, 3 - transmitted arc source, 4 - non-melting electrode, 5 - plasma gas, 6 - protective gas, 7- nozzle, 8 - protective cover, 9 - welded material

## Slide 117: Continuous beam welding - keyholing
FSW – Friction stir welding

## Slide 118: Welding parameters
FSW – Friction stir welding
Basic welding parameters:
Welding current (welding voltage)
- affects the properties of welds through plasma outlet pressure and temperature
Plasma gas flow rate
- is related to the kinetic energy of the arc and therefore also to the depth of penetration
Welding speed
The range should not exceed 20 to 30 cm/min - constant
Composition of plasma and shielding gases (+ flows) - constant
Welding wire feed speed
Burner setting and tungsten electrode type (nozzle diameter, burner distance)
Preparation of basic material

## Slide 119: Advantages of plasma welding
FSW – Friction stir welding
higher welding speed and the possibility of mechanization
smaller heat-affected area, and thus less deformation
smaller overhang of the weld, and thus a reduction in the laboriousness of the subsequent machining of the weld
maintaining favourable mechanical values of the base material
excellent weld appearance with easy reproducibility
excellent weld quality (high purity without pores and bubbles)
very good penetration and weld shape
reduction of laborious preparation of welded surfaces
it is not necessary to bevel the welded surfaces up to a thickness of 8 mm
can be welded in one pass and only on one side
saving additional material

## Slide 120: Areas of application of plasma welding
FSW – Friction stir welding
high quality and productivity of the process with minimal heat-influencing of the base material
nuclear industry
chemical industry
food industry
electronics
shipbuilding
aviation industry
automotive.

## Slide 121: Plasma cutting
Plasma cutting – designation:
According to ČSN EN ISO 4063:
- Method 83
PAC - Plasma Arc Cutting
-Thermal cutting process
If the plasma arc has a higher output velocity due to higher pressure, and the amount of gas supplied to the burner has a greater dynamic effect, the material gets cut.

## Slide 122: Plasma cutting - description of the method
FSW – Friction stir welding
The focused plasma beam heats a small area of material to be divided.
The beam temperature and heat flux are so high that the melting of the material occurs in the order of [ms].
The gas mixture together with the thermodynamic effect of the plasma blows the melt out of the cutting joint.
The resulting cutting joint divides the material.
Řezná
spára
Plazmová řezací hubice

## Slide 123: Types of cutting plasmas
FSW – Friction stir welding
This process is related to the physical properties of the gas:
Thermal conductivity
Heat capacity
Ionization energy
Energy of thermal dissociation of molecules
Gas plasma
Air plasma
Oxygen plasma
Nitrogen plasma

## Slide 124: Types of cutting plasmas
FSW – Friction stir welding
Gas plasma is stabilized with a mixture of Ar + H2; the electrode is tungsten and is mainly used for cutting high-alloy steels, nickel, molybdenum, copper and other metals.
Air plasma is currently very widespread; its operation is economically very advantageous up to a thickness of about 40 mm for cutting steel. Compressed air (0.4 to 0.8 MPa) with a high flow rate of up to 130 l.min-1 is used for stabilization.
Oxygen plasma is very similar to air but has higher enthalpy and density. Oxygen gives high cutting speeds, and clean cuts without adhering oxides, and increased cutting quality with a small deviation angle and fine surface structure.
Nitrogen plasma combined with an injectable water supply is designed primarily for cutting large thicknesses of high-alloy steels. Due to the design of the burner, water (sometimes carbon dioxide) is fed tangentially to the edge layers of the plasma beam. A water vortex is created, which cools the outer layers of the plasma and dissociates the water, which narrows the plasma and the temperature rises..

## Slide 125: The principle of cutting
FSW – Friction stir welding

## Slide 126: The principle of cutting
FSW – Friction stir welding

## Slide 127
FSW – Friction stir welding
Plasma cutting
Description of modern plasma cutting with high HD arc density

## Slide 128: Cutting burners
FSW – Friction stir welding
Robust burner for range 25-600 A
Robust consumables
High performance; the ability to cut in the thickness range 2-150 mm
Suitable for vertical and bevel cutting

## Slide 129: Technological possibilities and limitations of plasma cutting
FSW – Friction stir welding
Cuttable materials
Structural steels, High-alloy materials, Aluminium
Max thicknesses | standard |  | HD
Dividing cuts | 80 mm |  | 150 mm
Quality cuts | 50 mm |  | 120 mm
Cutting speed – plasmas Thickness of the material [mm] |  | Speed [mm·min-1] | 
5 |  | 7000 | 
20 |  | 2000 | 
50 |  | 400 | 
Cutting speed - plasma with high arc density
(High Definition - Hypertherm, Hi-Focus - Kjellberg, etc.)
0.5-8.0 mm (20-50A)
4-10 mm (50-100A)

## Slide 130: Technological possibilities and limitations of plasma cutting
FSW – Friction stir welding
The high temperature makes it possible to cut all conductive materials, regardless of their oxygen cutability
Plasma output velocity 1500-2300 m.s-1
The cutting speed is up to 10 times higher for thin materials compared to oxygen, but the speeds are equalized at thicknesses of 40-50 mm.

## Slide 131: Quality of the cut
FSW – Friction stir welding
20 mm carbon steel, 200 A cutting current
ESAB m3 plasma

## Slide 132
FSW – Friction stir welding

## Slide 133
FSW – Friction stir welding

## Slide 134: New process of plasma stabilization - water vapour
FSW – Friction stir welding
Voda
Pára
Plazma

## Slide 135: Advantages of plasma cutting
FSW – Friction stir welding
Higher cutting speed than oxygen cutting for thin and medium thicknesses
Reduction of heat introduced into the material - smaller TOO and deformation
Possibility of cutting all metal materials, especially high-alloy steels, aluminium, nickel, copper, and their alloys
Easy automation and mechanization
Minimal effect on surface quality of cut materials

## Slide 136: Disadvantages of plasma cutting
FSW – Friction stir welding
The cutting edge angle is larger than with oxygen cutting
The upper edge of the sheet is rounder than with oxygen cutting
High development of fumes, metal vapours, ozone and nitrogen oxides
High noise level from 80 to 100 dB
Intense UV radiation
High acquisition costs
Difficult to burn holes at thicknesses over 15 mm

## Slide 137
FSW – Friction stir welding
Thank you for your attention.

## Slide 138: 4. Laser Welding

## Slide 139: LASER - DEFINITION
LASER = quantum light generator
Equipment generating light having special properties based on stimulated photons emission

## Slide 140: LASER RESONATOR CONSTRUCTION
Laser medium - there is a jump of electrons between orbitals and the generation of photons, the so-called ACTIVE ENVIRONMENT
Energy source for electron excitation
Mirrors that allow oscillations of photons and the formation of a laser beam
Fully reflective mirror R = 100%
Semi-transparent mirror R <100% (approx. 95%)
Active medium
Light beam
Fully reflective mirror
Semi-transparent mirror
Energy source
Resonator

## Slide 141: LASER RESONATOR CONSTRUCTION
3
4
1
4
5
2
6
– active environment
- semi-transparent mirror
- impermeable resonator mirror
- pumping (excitation) of the active medium
- movement of photons in the resonator
6 - output laser beam

## Slide 142: RESONATOR CONSTRUCTION: SOLID STATE LASERS
The active medium is a crystal - Nd: YAG, ruby, etc. The crystal must have the potential of high energy excitation and remain in an energetically excited state for a certain period of time.
The source of energy is most often light or laser lamp diodes. Possible resonator arrangement:
13/59
ZESÍLENÍ

## Slide 143: LASER LIGHT PROPERTIES
Coherence - waves coming from different places of a radiating body are called coherent if all waves have the same wavelength, the same direction and the same phase shift
Monochromaticity - (λ) - same wavelength of all radiation photons (with the same frequency)
Low beam divergence - low divergence, propagation in one direction, possibility of focusing to a very small point - at the focal length of the optical system
Radiation polarization

## Slide 144: Perfect beam control. Spatial beam focus
Time-focusing of pulses, very short pulses
High beam intensity
Possibility of very short pulses
Possibility to achieve high power density (up to 108 Wcm-2)
Use of different wavelengths - a wide range of applications

## Slide 145: SOURCES OF ELECTROMAGNETIC RADIATION
Laser
Natural light source
Technical light source
4/59

## Slide 146: Properties of laser radiation

## Slide 147: Properties of laser radiation
（zdroj：Yamada）
ＴＩＧ svařování
Plazmové svařování
Laserové svařování
（zdroj：Kutuna）
Plošná hustota energie zdroje energie
Tvar průvaru (nákres）
laser
elektr. svazek
plazma
oblouk

## Slide 148: Laser beam transmission methods

## Slide 149: TRANSMISSION METHODS AND BEAM FOCUSING
Through lenses
(transparent optics)
With mirrors
(reflective optics)

## Slide 150: Laser beam focusing

## Slide 151: Laser comparison - beam quality
𝑑 = 4 ∗ 𝑀2 ∗ 𝑓 ∗ 𝜆
𝜋𝐷
What matters is the ability to focus the laser beam (area energy density):
Focus grows with:
f - lens focal length
λ - wavelength
M2 - beam propagation ratio; how close the beam is to the ideal Gaussian beam
Focus decreases with:
D - beam diameter in front of the lens

## Slide 152: Transverse modes - radiation energy distribution in a resonator

## Slide 153: Advantages and uses of laser systems
High power density corresponding to TEM
Efficient parameters of the active environment (temperature, pressure, consumption, etc.)
Required size of the impact area
Accuracy of reproduction of technological parameters
USE:
welding
cutting, drilling, marking, engraving, heat treatment

## Slide 154: Interaction of laser radiation with material
Transmission
Quarry
Reflection
Absorption
Incident beam
L+O+A+T=1
Laser beam absorption for various materials
Various materials; bodies have significantly different optical properties, which significantly affect energy absorption.
Material Surface treatment Temperature Radiation wavelength

## Slide 155: Interaction of laser radiation with material

## Slide 156
Interaction of laser radiation with material
Závislost absorpce na teplotě (Anomální absorpce)

## Slide 157
Electromagnetic spectrum of radiation
PROPERTIES OF ELECTROMAGNETIC RADIATION

## Slide 158: TYPES OF LASERS
Depending on the type of active environment:
Solid state matters – Nd3+:YAG,
Yb:YAG, ruby
(welding, cutting, marking, drilling, etc.)
Gaseous state matters – CO2, Ar, He-Ne
(cutting, welding, measuring, marking)
Excimer matters – mostly gaseous compounds, KrF, XeF
(medicine, etc.)
Semi-conducting materials – AlGaAs, GaN
Other - a laser on free electrons

## Slide 159: TYPES OF LASERS

## Slide 160
Classification of lasers
Classification of lasers

## Slide 161: Solid state laser : Nd3+:YAG LASER
Utilization of energy emitted by the lamp for pumping of crystal:
Active environment: YAG - Yttrium-aluminium garnet
doped with Neodymium

## Slide 162: Solid state laser scheme
– active environment
- semi-transparent mirror
- impermeable resonator mirror
- pumping (excitation) of the active medium
- movement of photons in the resonator
6 - output laser beam
3
2
4
6
1
4
5

## Slide 163: Nd3+:YAG LASER (solid state)
Scheme of solid-state Nd3 +: YAG laser with longitudinal excitation by semiconductor laser:
Scheme of solid-state Nd3 +: YAG laser with transverse excitation by semiconductor laser:

## Slide 164: Nd3+:YAG LASER (solid state)
Construction scheme of pulse Nd3 +: YAG laser ROFIN SINAR:
Construction scheme of continuous Nd3 +: YAG laser ROFIN SINAR:

## Slide 165: Examples of solid state laser systems

## Slide 166: Examples of solid state laser systems

## Slide 167: Gaseous state lasers - CO2
LASER
26/59

## Slide 168: Gaseous state lasers - CO2
LASER
TRUMPF
Source TLF 20 kW
Active medium: Gas mixture N2, CO2, He

## Slide 169: Gaseous state lasers - CO2
Mirrors
Energy source
HF electromagnetic waves
Active medium
– CO2
LASER

## Slide 170: CO2 LASER (gaseous state)
Scheme of CO2 laser with slow axial flow of the active medium:
Scheme of CO2 laser with fast axial flow of the active medium:

## Slide 171: CO2 LASER (gaseous state)
Scheme of CO2 TEA laser with transverse flow of active medium:
CO2 laser resonator = gaseous active medium

## Slide 172: Examples of gas laser systems
FSW – Friction stir welding

## Slide 173: SLAB Laser

## Slide 174: SEMICONDUCTOR LASER
Energy bands of the atom
GaAs laser diode
Semiconductor laser
Rofin Sinar DL 015:

## Slide 175: DIODE LASER
Individual diode
Creating a series of diodes by steaming
Connection of series into modules
The diode laser acts as a P/N diode that uses specific materials as active environments.

## Slide 176: New types of LASER construction

## Slide 177: Disk laser

## Slide 178: Disk laser

## Slide 179: Fibre laser

## Slide 180: Fibre laser

## Slide 181: Comparison of parameters of the most used lasers

## Slide 182: APPLICATION OF LASERS
Production technology
thermal separation (cutting)
welding
drilling
surface treatment of materials
(surface hardening, coating)
description
Medical applications
Measuring equipment
Printing and imaging methods
Research, development

## Slide 183: LASER WELDING METHODS
FSW – Friction stir welding
By conduction - at low power densities, heat absorption by the surface and its conduction into the material (usual penetrations up to 2 mm). Low energy absorption. For thin materials. Metal melting only.
Keyhole welding
Power density > 106 W.cm-2, evaporation of part of the material in the focus; the formation of plasma facilitates heat absorption - a step increase in absorption; the formation of a needle-like gap in the molten material further increases the absorption and deepening of the gap. Energy absorption up to 95%.

## Slide 184: LASER WELDING
FSW – Friction stir welding
Centrolaser.it

## Slide 185: LASER WELDING
Focusing the laser beam creates a place with a power density of up to 10MW.cm-2.
Formation of a melting bath.
Advantages:
Chemically clean heat source
Welding depth to weld width ratio (5:1)
Welding without additional material, weight reduction
Small heat-affected weld area, small deformations - no straightening
High weld quality - strength, no pores
High welding speed
Easy to use - automation
Universal - thickness 0.1-10 mm

## Slide 186: Comparison of shielding gases
during welding
welded material
laser beam parameters:
welding speed
working gas:
Argon – heavier than air
(good weld protection); easily ionizes (loss of E)
Helium - transmits more energy; greater penetration
Nitrogen – protects against oxidation; can also increase strength

## Slide 187: WELD GEOMETRY DURING THE WELDING PROCESS
mostly without additional material
joint of set sheets max. 0.1-0.2 mm; otherwise the beam passes through, the melt does not bridge the distance and flows away
in special cases, a joint is necessary - welding of galvanized sheets
possibility of using additional wire (during aluminium welding, surfacing), bridging wider joints - difficult to bring the wire exactly into the focus
Butt welds:
Precise assembly and inspection of the joint trajectory required (welding heads with camera)
Small area of molten material
High welding speeds
Deep penetration, strength
Overlap welds:
Larger area of molten material
Greater production and assembly tolerances - higher variability
Smaller strength

## Slide 188: THERMAL EFFECT OF THE BEAM DURING THE WELDING PROCESS
Possibility of cracks in stainless steel
Formation of martensite; brittleness
Good mechanical properties of fast-setting metals -Ti
Stainless steel is not prone to intergranular corrosion
Small TOO
Small deformations
Very fast cooling of the material causes:
Disadvantages:
Advantages:

## Slide 189: Welding and surfacing

## Slide 190: (Micro) surfacing

## Slide 191: USE OF LASER WELDING IN INDUSTRY
The share of special materials is growing in industry - high-strength steels, Al, Ni, Ti
Less influence of physical properties compared to conventional technologies
Relative independence from material properties - heat conduction
Joining various materials
Possibility to weld difficult-to-weld materials

## Slide 192: USE OF LASER WELDING IN INDUSTRY
Transport: vehicle body, exhausts and roof; speed, easy overlapping
Option: tailored blanks, remote welding
Aerospace industry: parts of turbines - connection of specific materials; now, also construction of drones - substitute for riveting

## Slide 193: THERMAL PARTITIONING OF MATERIALS BY LASER
High quality of the cutting surface of the parallel edge, without the need for finishing
Speed and quality are not affected by material hardness; low dependence on mechanical properties
Small heat-affected zone; heat-affected material is blown away
Shape variability - 2D cutting
Robotic 3D cutting
High cutting speeds compared to other cutting technologies
No mechanical deformation
Processing of surface-treated sheets - Cutting joint (0.1-0.4 mm)
31/59

## Slide 194: LASER CUTTING PRINCIPLE
The laser beam is focused by the lens into a small area, thus obtaining a high power density. The temperature rises in the impact area.
The cut material is heated above the melting temperature and sometimes above the evaporation temperature.
The assisting gas blown by the outlet nozzle to the point of interaction of the laser beam with the material blows the melt and vapours away from the point of cut.
If oxygen is used as the assisting gas, the material is also combusted after heating to the ignition temperature and the resulting oxides are blown away by oxygen pressure.
The combination of these processes creates a cutting gap in the direction of the burner movement.
33/59

## Slide 195: THERMAL PARTITIONING OF MATERIALS BY LASER
Principles of cutting joint formation:
sublimation (evaporation of material)
material melting (melt blowing away with assisting gas)
oxidation of material (using assisting gas - oxygen)
Process features:
high cutting power (high cutting speeds)
narrow cutting joint
minimum heat-affected area
process accuracy
possibility to cut different types of materials (metals, plastics, textiles, wood, glass, etc.)
limited material thickness (approx. up to 100 mm)
large thickness - low cut quality

## Slide 196: LASER CUTTING METHODS
Heat application to the material:
Melting
Combustion
Sublimation
Oxidative cutting – working gas O2 (1-5 bar)
Combustion: 4Fe + 3O2🡪 2Fe2O3 + E
Application: structural steels, thickness up to 40 mm
Melt cutting – working gas N2 (10-20 bar)
Energy only from the beam, molten material blown away by gas
Application: stainless steels, thickness up to 25 mm
Sublimation cutting – gas N2, for non-fusible materials
Usage: wood, paper - mostly cut in layers (slower); precise; special applications: ceramics, PCD

## Slide 197: LASER CUTTING PRINCIPLE

## Slide 198
THE IMPORTANCE OF THE FOCUS POSITION WHEN LASER CUTTING
The focus position depends on the type of material being cut and the technology used.

## Slide 199: Cutting and drilling

## Slide 200: LASER CUTTING - COMMON MATERIALS
FSW – Friction stir welding
METALS:
Construction steel
Stainless steel
Aluminium
Other
PLASTICS:
Plexiglass
PE
PP
Rubber
OTHER:
Textile
Skin
Glass
Composites

## Slide 201: LASER CUTTING - SPECIAL MATERIALS
cutting CBN, PKD inserts, chip breakers
Composite materials
semiconductors, capacitors–Si, GaAs
Stainless steel, NiTi stents

## Slide 202: LASER CUTTING IN 3D
Processing of bodies, parts made by moulding
CO2, Nd:YAG lasers, fiber lasers
Sheet metal: 1-4 mm
Speed: 2-5 m.min-1
Special optics according to the type of laser
Integrated distance sensors
Nozzles from the sheet metal surface
Autofocus
Emergency sensor

## Slide 203: Description, marking and engraving

## Slide 204: Heat treatment

## Slide 205: Micromachining

## Slide 206: Hybrid technologies
Laser - MIG

## Slide 207: HYBRID WELDING PROCESSES - COMPARISON
LASER
MAG
LASER + MAG
LASER + MAG
DEPTH AND WIDTH OF WELD: 4 kW CO2 laser, 8 mm carbon steel, sheet metal weld
LASER

## Slide 208
Thank you for your attention.

## Slide 209: ELECTRON BEAM WELDING
FSW – Friction stir welding

## Slide 210: Electron beam welding
Method designation according to
ČSN EN ISO 4063:
- Method 51
EBW =
Electron Beam Welding
Principle of the method:
It is a fusion welding process in which thermal energy is generated by the impact of a focused electron beam on the welded material.

## Slide 211: Principle of electron beam welding
The emitted electrons are supplied with high kinetic energy by an electric field (high voltage), which changes into thermal energy due to their impact.
In order to achieve a high thermal efficiency of the electron stream, the electrons are formed simultaneously during acceleration in a vacuum into a very thin beam.
This gives a highly concentrated heat source suitable for welding.

## Slide 212: Power density vs. weld shape

## Slide 213: Electron emissions
Electron emission is described by Richardson and Thompson as follows:
where:
Je = emission current density
A = emission constant (depends on surface emissivity)
T = absolute cathode temperature
e = base of natural logarithm
e.ϕo = output work of the electron from the metal
k = Boltzman constant
The velocity of electrons is given by the relation:
where: U = accelerating voltage

## Slide 214: Types of electrodes
Thermocathodes
a) directly heated metal strip cathode
b) directly heated V-shaped cathode
c) lanthanide boride cathode with indirect heating
d) directly heated metal cathode in the shape of a flat spiral
e) flat cathode with electron heating
f) rod cathode with electron heating

## Slide 215: Acceleration of electrons
The acceleration of electrons in vacuum is achieved by a high voltage which creates a potential of 30 to 200 kV between the cathode and the anode.
When an electron passes through a homogeneous electric field, it gains kinetic energy.
The calculation of the kinetic energy of electrons is also based on the relation:
Wk = 1/2 me. ve2 = e .U

## Slide 216: Principle of electron beam welding
Prerequisites for the creation of the EC
For welding, it is necessary to obtain free electrons and give them high speed.
Free electrons are obtained by heating the cathode, which emits electrons.
The acceleration of the electrons is ensured by an electric field and the use of a vacuum.
The electrons emitted are, due to an electric field (high voltage),
supplied with high kinetic energy.
This changes into thermal energy after the impact of electrons.
In order to achieve high thermal efficiency of the electron stream, the electrons are formed at the same time as they accelerate in a vacuum into a very narrow beam.
Electron focusing is achieved using magnetic fields.

## Slide 217: Electron beam welding scheme
An electron beam is formed in a so-called electron gun (nozzle).
The electron gun is powered by a high-voltage DC source.
Part of the electron gun is a cathode, located inside the focusing electrode.
This forms an electric field concentrating the beam into the anode hole.
An accelerating electrode (anode) is placed at a certain distance from the cathode.

## Slide 218: The principle of electron beam focusing
The electrons have the same charge, so they repel each other.
The beam diameter increases, and the beam energy decreases.
In order to increase the energy density in the beam after passing through the anode, the electrons are focused by a magnetic field in a special magnetic lens.
Due to the movement of the electron beam across and along the weld axis, a magnetic deflection system is inserted into the electron gun.

## Slide 219: Focusing principle
of the electron beam

## Slide 220: Electron beam interactions
These devices can weld with a very narrow beam with a diameter of up to 0.05 mm.
Material thicknesses are usually in the range of 0.1 to 50 mm, but with a horizontal weld position, thicknesses of up to 400 mm can be welded.
By electron beam welding at high voltages, it is possible to obtain a narrow and deep penetration.
During welding, the metal melting zone is preferably extended in the direction of the EC action.
a - energy distribution in the electron beam
b - form of remelting of the base material
c - electron beam energy distribution in the melting region

## Slide 221: Horizontal arrangement of devices

## Slide 222: Electron beam interaction with material

## Slide 223: Electron beam interactions

## Slide 224: Welding parameters
Acceleration voltage (kV)
Electron beam power (kW)
Electron beam current intensity (mA)
Welding speed (cm.min-1)
Electron beam trace diameter (mm)
Vacuum size (Pa)
The distance of the electron beam outlet from the electron gun

## Slide 225: Dependence of weld penetration depth on the amount of heat introduced

## Slide 226: Material weldability
Electron beam welding is characterized by depth weld penetration with a very narrow metal melting area; there is no need to use additional material to fill the weld gap.
By modifying the chemical composition of the weld metal with an additional material of suitable composition, it is possible to address the issues of improving the mechanical properties of the weld metal, increasing the resistance to cracking, etc., e.g., when welding combined materials.
Additional material can be used in the form of wire, tape, powder, etc.

## Slide 227: Examples of applications

## Slide 228: Examples of applications

## Slide 229: Advantages of electron beam welding
deep weld penetration and very good weld appearance with a fine surface drawing
narrow molten and heat-affected area
small deformations
perfect protection of the weld from the air atmosphere, and good refining effects of the vacuum
possibility to weld larger thicknesses of materials in one pass
of the electron beam mostly without the need for additional material (keyholing)
the possibility of a high degree of automation of the welding process
easy and programmable beam power control
possibility to weld in places inaccessible to classic technologies
possibility of energy transfer, even at a distance greater than 500 mm
possibility of use for a wide range of materials and their combinations

## Slide 230: Disadvantages of electron beam welding
only a small percentage of the total time is used for welding
demands on the cleanliness of welded materials
need for vacuum
unfavourable nature of primary crystallization of weld metal, especially in connection with the issue of cracking of welded joints
requirements for accuracy (and cleanliness) of welded surfaces
demands on the accuracy of the beam management
relatively high investment costs for welding equipment

## Slide 231: Occupational safety and hygiene
High voltage work - must comply with electrical and technical regulations
Secondary phenomenon - X-rays occur
(in terms of the biological effect of radiation on the surface of
the welding device, radiation dose must not exceed the prescribed value)
It is necessary to follow the principles for working with ionized radiation
Materials that evaporate easily in a vacuum should not be welded with an electron beam (among other things, they contaminate the vacuum chamber).Brass, zinc, cadmium

## Slide 232: Examples of welding equipment

## Slide 233: Basics of SOLDERING

## Slide 234: Definition of soldering
Soldering is a method of metallurgical connection of metallic or non-metallic materials using molten filler material where there is no melting of the base material (but only wetting with molten solder).
Additive material = solder - must have a melting temperature lower than ZM

## Slide 235: Technology comparison: welding vs soldering
WELDING
High heating - above melting temperature
PM may or may not be used
The chemical composition of PM is close to the composition of ZM
Local heating
Deformation vs. residual stresses
SOLDERING, BRAZING
PM must be used (= solder)
Solder has a lower Tt than ZM - different chemical composition from ZM
Low operating temperatures (material does not heat up to Tt)
Price
Favourable in terms of deformations and internal stresses

## Slide 236: Use of soldering
Soldered joints are most often used in cases where the following is required:
Tightness of the joint
Electrical conductivity
Corrosion resistance
Nice surface appearance (smooth transition to ZM)
Mechanical strength at static (dynamic) load
When creating complex joints
When creating heterogeneous connections
(ferrous vs. non-ferrous, metallic vs. non-metallic)
Wherever fusion welding cannot be used
(for metallurgical or technological reasons)

## Slide 237: Use of soldering
Currently, soldering is used for joining ferrous and non-ferrous materials, as well as complex products:
Non-alloy structural steels - solderability depends on C content (Cu Ag-based solders)
Alloy structural steels - solderability depends on the content of alloys (Cu, Al, Ti, Si, Mn, etc.); they form stable surface oxides; it is necessary to create special technological conditions (heating rate, cooling, choice of suitable flux and reducing atmosphere)
Refractory and heat-resistant steels
Stainless steels
(Ni-based solders)

## Slide 238: Use of soldering
Can also be used for high-strength alloys, non-ferrous metals and wherever fusion welding cannot be used:
Cast iron
Copper and its alloys
Aluminium and its alloys
Nickel and its alloys
Titanium and its alloys
Other metals (Ag, Au, Pt, Pd, Be, Mo, Zr, Nb, W, etc.)
Ceramics
  WC, TiC, TaC, Cr3C2 – connecting metal Co
  Al2O3 – Ti, AgCuTi-based solders

## Slide 239: Types of soldered joints
1 - overlapped connection
2, 3 - butt joint
4 - oblique joint
5 - butt joint with attachment
6 - overlapped hemmed joint
7, 8 - overlapped fitted joint
9 - profile soldering
10 - folded joint
11 - external socket pipe connection
12 - blunt socket joint
13 - overlapped socket joint

## Slide 240: Types of soldered joints

## Slide 241: Mechanical properties of soldered joints
The mechanical strength of soldered joints depends on the properties of the parent metal, the construction of the joint, solder, flux and the soldering process.
The size of the gap between the soldered components and the areas of their overlap have the greatest influence on the strength.
The mechanical properties of the solder change during the soldering process.
The most important area of the joint from the point of view of strength is the layer formed by diffusion: this grows with the temperature and time of action of the solder - in the range of 0.1 to 1000 μm.
The mechanical strength of the joint is proportional to the mechanical strength of the solder.
Solders with a eutectic composition have the greatest mechanical strength.
The strength of soldered joints decreases with ageing time, higher operating temperature and increasing dynamic stress on the joint.

## Slide 242: Physical nature of soldering
During soldering, complex physico-chemical processes take place at the solid-liquid interface.
The molten solder in the wetting area implements the bond between the solid phases of the base materials.
The heat increases the movement of the atoms of both phases, and their mutual diffusion strengthens the formed bonds.

## Slide 243: Physical nature of soldering - diagram of a soldered joint
It consists in wetting ZM in the solid state with liquid solder (PM).
Conditions for the formation of adhesive forces are created between the ZM atoms and the solder.
Dissolution and diffusion of ZM and solder atoms occurs.

## Slide 244: Diffusion
- The condition for diffusion during soldering is the displacement of solder atoms (PM) and ZM - conditioned by their inhomogeneity
Diffusion in the soldered joint changes the chemical composition of the solder and ZM, creating transition areas.
The direction of movement is given by the concentration gradient. Diffusion is affected by structural defects, temperature gradient, activity, etc.
The diffusion area is the most important in terms of strength.
The thickness increases with temperature and soldering time.
It is more fragile than ZM and PM.
The goal is to make the joint not brittle.

## Slide 245
Diffusion
Using the basic diffusion equations, the dependence of the diffusion coefficient D on the temperature t was empirically determined: 𝑄
𝑘. 𝑡
𝐷 = 𝐷0. 𝑒𝑥𝑝 −
where: D0 is the frequency factor, Q is the activation energy of diffusion, k is the Boltzmann constant.
The depth of the diffusion layer X can be expressed using the 2nd Fick law depending on the diffusion coefficient (D) and time (t).
Where x is the diffusion depth (cm)
D is the diffusion coefficient(cm2.s-1) td is the diffusion time (s)
2
𝑥 = 2𝐷. 𝑡𝑑

## Slide 246: Solder joint structure
Transition areas
  Mechanical, chemical and physical properties other than ZM
  The higher the solubility of solder and ZM, the wider the transition areas
Formation of the intermediate phase
  Reaction of liquid solder and ZM
  Partial dissolution of ZM and elimination
  of the intermediate phase at the boundary of solid ZM
  By cooling the joint and heat treatment
1 = base material (ZM), 2 = transition area ZM,
3 = transition area solder, 4 = solder

## Slide 247: Physical nature of soldering materials
Most soldering techniques use capillary forces to form the joint.
Only during deposition soldering does the solder reach the soldered surface by mechanical interaction (e.g., soldering iron tip).
CAPILLARY SOLDERING
It uses capillary pressure to transport solder to the joint, which is significantly manifested at gaps between the connected parts smaller than 0.5 mm.
- Capillary pressure forces the solder (or flux) to fill the gap in all directions.
- In order for this to happen, the following must be met:
- ZM, solder and flux must be heated to operating temperature
- ZM and solder must have good wettability and capillarity

## Slide 248: Soldering operating temperature
The operating temperature is selected according to the type of soldering used.
For capillary soldering, it is selected in the range of 20 to 100°C above the liquid solder used.
For deposit soldering, the minimum soldering temperature is equal to the wetting temperature (the surface wets but does not melt).
According to the melting temperature (solidus) of the solder, we divide the soldering into:
Soft soldering (Tt solders below 450°C)
Hard soldering (Tt solders above 450°C)

## Slide 249: Physical nature of soldering - surface tension /N.m-1/
The so-called surface tension in the contact surfaces between solid material, liquid solder and flux or protective atmosphere (or vacuum) plays an important role in soldering.
PN affects the wettability, flowability and capillarity.
The size of PN of molten metals depends on:
    Their structure
Temperature
Flux composition, atmosphere
Lots of active solder elements

## Slide 250: Physical nature of soldering - surface tension /N.m-1/
Inside the liquid (molten solder), the attractive forces of the particles cancel each other out and create an equilibrium state.
The molecules on the surface of the liquid are not symmetrically surrounded by other atoms.
Intermolecular forces draw them inward.
Trying to occupy a minimum surface area, i.e., resulting in the effect of forces acting on the surface = surface tension.

## Slide 251: Physical nature of soldering - Wettability
- The ability of liquid solder or flux to adhere to the surface of ZM at a certain temperature

## Slide 252: Physical nature of soldering - Wettability
The ability of liquid solder or flux to adhere to a clean ZM surface at operating temperature
During wetting, a drop of molten solder assumes such a surface shape that the energy of the system ZM - solder - flux (atmosphere, vacuum) is minimal, and interatomic forces can be applied.
There are three types of forces at the junction:
Adhesion forces (attractive forces of the atoms of the surface layer of solid ZM and liquid solder)
Cohesion forces (attractive forces of neighbouring atoms in liquid solder)
Attractive forces of gaseous environment atoms

## Slide 253: Physical nature of soldering - Wettability

## Slide 254: Physical nature of soldering - Wettability

## Slide 255: Physical nature of soldering - Wettability
The following equations apply to point A:
The following applies to the contact angle of wetting:
(sigma H = adhesive stress)

## Slide 256: Physical nature of soldering - Wettability
A decrease in surface tension (Sigma 23) and interfacial tension (Sigma 12) and an increase in Sigma 13 tension have a positive effect on wettability.
The magnitude of these stresses can be affected by:
The right choice of temperature
The type of flux
Alloying ingredients in solder
Wettability and flowability can be improved by a small amount of additives such as: Pd, Li, Ni, Si, Mn, Be, V, B, P.
As the mutual solubility of solder and ZM increases, the wettability improves.

## Slide 257: Physical nature of soldering - Flowability
Flowability is the ability of solder (or flux) to spread over the horizontal surface of the base material.
The size is given in mm2 of the area occupied by a precisely defined solder sample after heating according to the specified technological procedure.

## Slide 258: Physical nature of soldering - Capillarity
- The ability of liquid solder at a certain temperature to fill a narrow joint gap by capillary forces

## Slide 259: Physical nature of soldering - Capillarity

## Slide 260: Physical nature of soldering
Solder - additive material - melting temperature below the melting temperature of ZM.
Flux - a chemical agent that helps soldering

## Slide 261: Physical nature of soldering
Flowability
The ability of a liquid solder or flux to melt at a certain temperature on a horizontal surface of ZM
Capillarity
The ability of liquid solder to fill a narrow gap between
soldered parts (by capillary forces)
Solder - additive material - melting temperature below the melting temperature of ZM.
Flux - a chemical agent that helps soldering

## Slide 262: Advantages of soldering vs
Disadvantages of soldering
High productivity (t less than 2 mm)
Possibility of process mechanization
Connecting by combined ZM
  Non-metal ZM
Gradual soldering
  Graduation of PM according to operating temperature
High-quality reproducibility
  Low inspection costs
Connecting different thicknesses
Lower thermal energy consumption
  Diffusion joint
Ecological working environment
Less internal stress; great dimensional stability
Lower joint strength
Susceptibility to corrosion
    Presence of additional material in the joint
Demands for precise joint preparation - more labour
High equipment and soldered products costs

## Slide 263: Preparation of soldered materials
To create the perfect connection, it is necessary to ensure the following preparatory operations:
-Degrease the surface with a suitable degreaser
(acetone, gasoline, thinners, etc.)
-Surface treatment
(grinding, blasting vs. pickling and neutralization)
- he soldered joint is a material notch with a sudden change in cross-section and voltage peak
- i.e. overlapped joints are most preferred
Adjustments after soldering:
- Removal of flux residues, rinsing with water, TZ

## Slide 264: Soldering procedure
In order to create a quality soldered joint, it is necessary to follow a certain sequence of operations and measures (the cleanliness of soldered surfaces is also important).
-Choose the combination ZM - PM (solder) - flux correctly
(usually as recommended by solder manufacturers).
-Ensure the mutual position of the parts before soldering so that there is no uncontrollable displacement of the parts during soldering or cooling of the joint - (frequent use of jigs).
-Choose a suitable preheating procedure (should be fast, otherwise there is a risk of flux degradation).
-Create optimal conditions for solder to flow into the joint.
-Carry out cooling and finishing the joint in a suitable way.

## Slide 265: General requirements for solders
the melting temperature of the solder must be lower than the melting temperature of ZM
the melting interval should be narrow - for capillary soldering (max. 100°C, or the eutectic composition of the solder is chosen); otherwise liquidation occurs and the material is insufficiently fluid and does not fill the gap perfectly
must have good soldering properties (wettability, flowability, capillarity); in the molten state, it should have a low surface tension (but may not have the same chemical composition as ZM)
solder and ZM elements must have mutual (partial) solubility to form solid solutions; solder elements must not form brittle intermediate phases (ZM must also have a low content of impurities)
due to corrosion, the solder should contain elements with little difference of electrochemical potential with ZM used

## Slide 266: Types of solder design
Solders should have good mechanical properties
Solders are produced in the form of:
-sticks, wires, filled tubes
-thin sheets, foils, tapes
-powders, pastes
-wire rings
-circular profiles

## Slide 267: Types of solder design

## Slide 268: The issue of introducing lead-free solders
CONTAIN: tin, copper, silver, bismuth, indium, etc.
The melting temperatures of lead-free solders are higher than those of leaded solders.
E.g. SnAg solders have a melting point of about 220 to 250°C - (Sn63Pb37 eutectic solder has a melting point of 183°C).
Higher solder melting temperatures - increased oxidation of solder and soldered surfaces.
»Consequence - poorer wettability of the soldered joint.
Reduction of oxidation - use of more active fluxes.
»Consequence - flux residues can be poorly removed (negative impact on joint reliability.
The price of lead-free solders is usually higher.

## Slide 269: Types of solders - brazing
According to the relevant standard ČSN EN 1044, we divide brazing solders into 8 groups according to the main alloying element.
AL - containing aluminium as the main ingredient
AG - containing silver (not the main element, but a significant ingredient)
CP - containing copper as the main element, and the additional element is PHOSPHORUS (P)
CU - containing copper as the main ingredient; solder is not included in group CP
NI - containing nickel as the main ingredient
CO - containing cobalt as the main ingredient
PD - containing palladium in any amount
AU - containing gold in any amount
+ a three-digit number specifying the type of solder in the group

## Slide 270: Types of solders - brazing (according to the standard ČSN EN 1044)
Copper (CP) - manufactured on the basis of Cu-P
use for soldering copper and its alloys
not suitable for steels and alloys with more than 10% Ni (brittle transition areas are formed)
Solder copper must be pure, oxygen-free. The phosphorus additive acts when heated to the working temperature by breaking up the oxide layer on the copper surface (it is then not necessary to use flux when soldering Cu + Cu). However, due to the formation of a brittle transition phase, it is suitable that the solder also contains Ag.
Copper – brass (CU) - based on Cu-Zn (MS60 - 60% Cu) with addition of other alloys: Sn, Si, Ag, Ni, Mn (Zn content up to 40%)
working temperature approx. 900°C; the use of flux is necessary
are the most used (do not form fragile phases, have good
soldering properties and sufficient bond strength) for soldering steels, copper, and their alloys

## Slide 271: Types of solders - brazing (according to standard ČSN EN 1044)
Silver (AG) – produced on the basis of Ag with the addition of Zn, Cu, Cd, Mn
soldering of stainless steels (austenitic)
heat resistance up to 500°C,
= used for soldering virtually all ferrous and non-ferrous metals
(excluding light metals, except titanium and its alloys)
they are relatively expensive
Aluminium (AL) - produced on the basis of Al-Si, or Al-Si-Cu, Al-Si-Mg
- use for soldering aluminium and its alloys
Nickel (NI) - based on Ni + B, P, Si, Cr
suitable for soldering refractory, heat-resistant and stainless steels and alloys

## Slide 272: Types of solders - brazing
Palladium (PD) – heat resistant solders
- use for components of gas turbines, aircraft, nuclear
reactors
Gold (AU) – based on Au + Ni, Cu
- use in dental technology and in goldsmithing

## Slide 273: Distribution of fluxes - brazing (according to standard ČSN EN 1045)
1) FH - fluxes for brazing heavy metals (includes 7 types of fluxes)
FH10 = temperature range 550-800°C, for general use, residues
corrosive
FH 11 = temperature range 550-800°C, for Al-Cu soldering
FH 12 = temperature range 550-850°C, for alloy steels, corrosive residues
FH 20 = temperature range 700-1000°C, for general use, residues
corrosive
FH 21 = temperature range 750-1000°C, for general use, corrosive residues
FH 30 = temperature range above 1000°C, for Cu, Ni, non-corrosive residues
- FH 40 = temperature range 600-1000°C, contains chlorides, fluorides, but without boron, corrosive residues

## Slide 274: Distribution of fluxes - brazing (according to standard ČSN EN 1045)
2 ) FL - fluxes for brazing light metals (includes 2 types of fluxes)
- FL10 = lithium chlorides and fluorides, corrosive residues
- FL 20 = non-hydroscopic fluorides, non-corrosive residues

## Slide 275: Examples of fluxes

## Slide 276: Division of soldering methods
Depending on the soldering temperature
Soldering (solder melting temperature up to 450°C)
Brazing (solder melting temperature above 450°C)
According to the purpose of use
Connecting
Sedimentary
Definition in ČSN EN I4324

## Slide 277: Division of soldering methods
According to the shape of the joint
Capillary soldering - filling the gap with liquid solder occurs by the effect of capillary force (rising) in the narrow gap of the joint
Bevel soldering - the joint is made by applying individual solder beads without the effect of capillary forces
According to the method of adding solder
Soldering with the addition of solder during soldering
Soldering with pre-inserted solder
According to the method of heating
  Soldering with direct heating
  Soldering with indirect heating (via pad, etc.)

## Slide 278: Division of soldering methods
Depending on the type of environment
Soldering in air
In a protective atmosphere (hydrogen, helium, nitrogen)
In a vacuum
According to the working manner
Manually
Mechanically
According to the heat source
- With solder, flame, immersion, induction, electrical arc, etc.

## Slide 279: Designation of soldering methods according to standard ČSN EN ISO 4063
9 – Hard soldering (brazing), soft soldering and bevel soldering
91 - Brazing
911 - Infrared brazing
912 - Flame brazing
913 - Furnace brazing
914 - Brazing
915 - Brazing
916 - Induction brazing
918 - Resistance brazing
919 - Diffuse brazing
924 - Vacuum brazing
93 - Other brazing methods
94 – Soft soldering
947 - Ultrasound soft soldering
951 - Soft wave soldering
952 - Soft soldering with a soldering iron
97 – Hard bevel soldering

## Slide 280
FSW – Friction stir welding
Thank you for your attention.

## Slide 281: RESISTANCE WELDING
VypAuracoval: Ing. Petra Janíčková
KódAu prezentace: OPVK-TBdV-METALO-STRS-2-STE-PJA-001
Technologie budoucnosti do výuky
CZ.1.07/1.1.38/02.0032

## Slide 282: Resistance welding
Definition of the method:
Resistance welding is a method in which the resistance (Joule) heat generated by the passage of the welding current through the materials to be joined that form part of the welding circuit is used.
After heating, the parts are compressed and welded.
Resistance welding methods belong to the group of pressure welding, because a force must be used to create a plastic deformation, and weld the part to create a welded joint.

## Slide 283: Division of resistance welding methods
According to the structural arrangement of the electrodes and the working procedure, we divide the methods of resistance welding into:
spot - welded joints are created in the form of welded lenses (spot welds) between overlapped parts
seam - welded joints are formed using disk electrodes usually between overlapped parts as continuous or intermittent
protrusions - welded joints are created in places of natural or intentionally created protrusions (sometimes referred to as press resistance welding)
joints - welded joints are created in the entire joint area with or without the use of the desoldering phase of the welding process, (i.e. desoldering and compaction welding)

## Slide 284: Method designation – according to standard ČSN EN ISO 4063
2 RW – Resistance Welding (AWS)
– RSW – Resistance Spot Welding
– RSEW – Resistance Seam Welding
– PW – Projection Welding
– FW – Flash Welding
– RBW – Resistance Butt Welding
291 – RSEW – HF – High Frequency Welding

## Slide 285: Range of basic parameters (21)
Welding position
Thickness range ZM
Type of basic material
Welding current range
Voltage range (secondary)
Welding current type
Welding time
Compression force
Electrode diameter
: all
: 0.4 to 4 mm or more
: non-alloy and alloy steels, Ni, Al, Cu and their alloys
: 1000-100,000 A
: 0.5-10 V
: AC and DC
: 0.04-2 s
: 500-10,000 N
: 2-3 mm and larger

## Slide 286: Resistance heating
Resistance welding uses the phenomenon that heat is generated when an electric current passes through a conductor.
In this method of welding, a weld is created when the current passes through the compressed welded parts due to the electrical resistance at the point of contact (so-called transition resistance).
As a result, the material of the welded parts heats up and becomes malleable or melts, after which the material is compressed to form a metallurgical joint.
The influence of the surrounding atmosphere on the quality of the welds is practically eliminated due to the pressing force that acts during the entire welding process.
Thus, heat is generated directly in the materials to be welded and is not supplied from the outside, as is usual with other welding methods (e.g. flame welding, electric arc welding, etc.).

## Slide 287: Resistance heating
FSW – Friction stir welding
The amount of heat Q is greater the greater the following factors are:
flowing electric current I [A]
electrical resistance of the conductor R [Ω] - consists of several partial resistors
current flow time t [s]
This dependence can be expressed mathematically by the so-called Joule-Lenz law in the equation:
Q = R.I2.t [J]
or [*0.24 cal]
In the practical use of this dependence for welding, the control elements of the welding source can affect: the current Isv, the current transit time tsv and the value of the pressing force Fsv, which partially affects the resistance R, which is otherwise fixed by the welded material and electrode types.

## Slide 288: Transitional and material resistances
At the weld site we can trace several partial electrical resistances,
whose sum forms the resulting resistance Rsv, which contributes to heat generation:
electrode contact resistances (Rd), which, in special cases, may differ and are undesirable in resistance welding;
actual resistances of the welded materials (Rm), which can also differ, either due to the thickness (or cross-sections) of individual parts or the internal resistance when welding unequal types of material;
resistances between welded materials (Rk), which are a function of thickness and resistance of the oxide layer, surface irregularities, magnitude of the pressing force, etc. = so-called transient resistances.
The resulting resistance can therefore be expressed by the relation:
Rsv = Rm1 + Rm2 + Rd1 + Rd2 + Rk

## Slide 289: Transitional and material resistances
Welding
source
Welding lens
Heat-affected area
Welding pressure force
= electrode resistance (Rd1)
= electrode resistance (Rd2)
= transitional resistance
= material resistance 1 (Rm1)
= transitional resistance (Rk)
= material resistance 2 (Rm2)
= transitional resistance

## Slide 290: Transitional and material resistances
The nature of the distribution of electrical resistance at the start of the welding process for individual methods of resistance welding:
Spot and seam
Protrusions
Flash welding
Butt welding

## Slide 292: Welding process metallurgy

## Slide 293: Welding process metallurgy
The formation of each spot weld is characterized by rapid heating in a confined space up to the melting temperature, followed by very rapid cooling.
This cycle takes place when the welded parts are constantly pressed together. The highest temperature is reached in the middle of the molten core.
The heating and cooling rates are very high and reach several thousand degrees per second (up to 100,000°C).

## Slide 294: Prerequisites for the formation of a weld
Requirements for the basic material Securing the passage of electrical current
Good electrical conductivity
Good malleability
Low thermal conductivity
Fusible weldability
Metal - clean transition surfaces
Sufficient welding electrode pressure
Scope of application of the process
Thickness
ZM
THE SMALLEST
EVERYTHING CAN BE ROLLED
THE BIGGEST
5-20 mm
USUALLY UP TO
5 mm
EXCEPTION
Al-alloys up to 5 mm

## Slide 295: Process characteristics (advantages vs. disadvantages)
Comparison with other welding technologies
Heat is generated directly in the joint
Absence of the surrounding air atmosphere (due to the derived electrode pressure)
No additive material is used
High pressure cooling
A large force is required to create a weld
High productivity (very short welding times)
Automatically controlled welding process (easy mechanization and robotization)
Susceptibility to corrosion is eliminated
Better mechanical properties (cooling takes place at high speeds)
The heating and cooling rates are high, i.e. Martensite is formed
(removes seam welding)

## Slide 296: Resistance SPOT welding
Spot welding is the most widely used method of resistance welding of sheets with a thickness of approximately 0.01 to 10 mm. (However, even larger thicknesses can be welded)
Electrodes
Pressure arms
Basic (welded) material
Weld
Welding source
Power switch
During spot welding, mainly lap joints are created.

## Slide 297: Principle of resistance spot welding
The highest temperature occurs at the point of contact of the sheets. However, a considerable amount of heat escapes by conduction into the material and radiation into the surrounding environment.

## Slide 301: Principle of resistance spot welding
After clamping and compressing the welded parts between the electrodes, the welding current circuit closes. The passing current heats the joint in approximately a column of the same diameter as the welding electrode.
As soon as the melting temperature is reached, a liquid core of the joint is formed and welding takes place. Then the welding current is interrupted, but the pressure persists, and the weld and its plastic surroundings solidify quickly.

## Slide 304: Distribution of spot welding - according to the arrangement of electrodes
1 - Spot welding, 2 - Welded material
3 - Current source, 4 - Rod electrodes
1 - Spot welds, 2 - Welded material,
3 - Current source, 4 - Rod electrodes,
5 - Conductive board
Direct
The electrodes are located on opposite sides of the welded parts
Indirect
The electrodes are usually placed on only one welded part and the other rests on a pad

## Slide 306: Multi-spot resistance welding
In addition to the classic arrangement, there are a number of others that allow for welding multiple spot welds at the same time (multi-spot welding).

## Slide 307: Welding parameters
Welding parameters for specific types of materials and their different thicknesses are usually arranged in a table and are part of the technical documentation for the welding source.
However, it should always be borne in mind that the data are essentially for information only and that several test welds need to be made for practical use.
The basic welding parameters for spot welding are:
  welding force (Fs)
  welding current (Is)
  welding time (ts)

## Slide 308: Influence of pressing force
The effect of pressure during the welding process can be divided into three consecutive time periods:
pressure
the pressing force improves the contact of the contact surfaces, and thus a more even transition of the electric current at the beginning of welding
welding
during the formation of the weld, the welding pressure maintains the pressing force of the molten metal in a closed cavity and prevents its spraying
forging (weld processing)
at this stage, the action of pressure improves the structure of the weld (softens the grain, removes imperfections) and thus increases its mechanical properties

## Slide 309: Welding mode
When setting the basic welding parameters, a large number of combinations of individual parameters are offered.
The interrelationship between the main welding parameters is referred to as the welding mode, and their time course as the welding programme.
Soft welding mode
is characterized by low welding current (current density up to 200 A/mm2) and long welding time (about 25 periods - 0.5 s to 1.5 s) with lower welding force (up to 1,000 N) - pressure up to 60 N/mm2.
Hard welding mode
is characterized by a high welding current (current density 200-500 A/mm2), short welding time (3 to 8 periods - 0.16 s) and higher welding force (approx. 2,000 N) - pressure more than 80 N/mm2.

## Slide 310: Optimal band for making welded resistance joints
- hard welding mode
- soft welding mode
A - zone with insufficient amount of energy needed for weld formation (area of diffusion joints)
B - area of combination of parameters at which we achieve good welds
C - area of combination of parameters where thermal energy is overloaded - molten material sprays out
I.
II.
B
A
C

## Slide 311: Hard welding mode
The current state of knowledge and practice clearly prefers hard welding modes.
Higher pressures are used; the electrodes do not wear out so much (reduction of the contact resistance Rd)
The electrodes heat up less - longer life
The mode has higher efficiency and higher productivity (shorter welding time), less heat loss - less TOO
Minor deformation
The disadvantage is the higher investment costs (the welding machine must be equipped with a pneumatic or hydraulic system to induce the appropriate pressure and electronic control)
Higher wattages and compressive forces - higher stresses in welded joints
The need for careful preparation of welded parts
This mode is selected when welding alloy steels, non-ferrous metals and their alloys

## Slide 312: Soft welding mode
The electrodes are unfavourably thermally stressed, so they degrade faster and require more frequent adjustment and replacement.
The deformations of the weld joint are larger, the electrode impressions are deeper and the weld structure is coarse-grained (less strong).
The advantage of this welding mode is that it reduces the risk of turbidity of the material, which is advantageous for steels with a higher carbon content.
Also suitable for repairs and processing of dirty sheets.
There is a small diameter of the welding lens, with noticeable bruises along the edge.
Higher energy consumption.

## Slide 313: Welding time course - Welding cycle
The correct ratio of the size of the resistance welding parameters is not a guarantee of a quality weld.
It also depends on their time course, the so-called welding programme.
All resistance welding machines are designed with the main technological principle:
"The welding current is introduced into the welded object only after reaching the appropriate welding force (Fs) with a certain time delay."

## Slide 314: Welding time course - Welding cycle
Time course of welding of one spot weld:
It can be seen from the course that the force Fsv rises to the required set value for the time period td - the settling time required to reach full pressure.
The set force value is maintained for the welding time ts . Only after the end of the interval ts (switching off the welding current), the force Fsv decreases back to the zero value of the interval tk - forging time, when the cooling weld metal is forged.
It is necessary that the force Fsv is not released before the end of the interval ts; otherwise there is a risk of cavities forming in the weld.
In addition, more complex welding programmes are used to include preheating, annealing, etc. during the welding process.

## Slide 316: Use of spot welding

## Slide 317: Resistance welding losses
Material resistance size + transient resistances
Rm = f (conductivity, thickness, quality, temperature)
Rp = f (purity, surface roughness, etc.)
1) By dissipating electric current through adjacent welds
2) Impedance of the secondary welding circuit (material mass, jigs, etc.)
3) Arm extension (depends on the size of the "welding - induction - window")
Definition according to 05 0003
Arm distance = the smallest clear distance between the arms of a resistance spot and seam welder or between the plates of a resistance protrusion welder
Arm extension = clear distance of the resistance welder from the axes of the point electrodes, clamping plates, or from the centre of the working surface of the discs to the nearest fixed obstacle on the machine
Welding (induction) window = product of unloading and arm spacing

## Slide 318: Influence of the arms of the welding source

## Slide 319: Resistance SEAM welding
Welding process similar to spot welding.
The main difference is that the welding electrodes are rotatable and have the shape of a disk (pulleys), between which the welded parts roll.
If the pulleys were stationary, only a single spot weld would be created, as with spot welding.

## Slide 320: Welding parameters of seam welding
The physical principle of creating a weld is the same as for spot welding.
However, the basic welding parameters are different:
welding current - usually up to twice that of spot welding
pressing force - greater than spot welding
welding speed (identical to the circumferential speed of the electrodes)
welding current modulation (= welding current flow interruption)
In this method of welding, it is also possible to use additional strips, which are inserted between the electrodes and serve as intermediate layers between the welded part and the electrode, and remain welded to the base material = use of PM.

## Slide 321: Modulation of the welding current
Seam welding creates either individual or overlapping spot welds.
Due to the nature of the contact of the disk electrodes with the welded parts and for the branching of the welding current, seam welding is used for welding sheets with thicknesses of 0.5 to 3.5 mm.

## Slide 322: Use of seam welding
As with spot welding, lap welds are created in this way, e.g., sealing welds on the edges of various tanks, radiator fins, etc.; edge welds can also be created.

## Slide 323: Resistance INDUCTION welding
Sometimes also called
High-Frequency Welding.
Induction welding uses the heat generated by induction in the welded edges of the butt weld of the sheets during the passage of medium or high-frequency alternating current.
Induction welding is mainly used in the production of welded pipes.
This method is classified as seam welding, but is, in fact, butt welding.

## Slide 324
Types (shapes) of used electrodes
Electrode types and their most used shapes

## Slide 325
FSW – Friction stir welding

## Slide 326
Types (shapes) of used electrodes
Different types of welding electrodes
Detail of cooling welding electrodes

## Slide 327: Electrode materials
Electrode materials are classified into two groups: A and B
(according to RWMA Resistance Welder Manufactures Association) and further into several subgroups (types).
A similar procedure for sorting electrode materials is maintained in the valid standard ČSN EN ISO 5182.
Group A includes the most used electrode materials based on copper and its alloys. The materials are prepared by hot forming, cold forming, or used in the cast state.
In group A, the materials are further divided into 4 types.
Group B includes materials made by refractory metallurgy based on refractory metals such as W and Mo.
There are a total of 6 types of materials in this group
CuCr - low-carbon steel
CuBeCo - alloy steels
CuAgCd - Cu alloys, Ni alloys

## Slide 328: Resistance PROTRUSION welding
Protrusion welding is performed on welding presses; the welding process is located in places of natural or intentionally created protrusions - also called "nipple welding”.
Before welding. After welding
highly productive welding method suitable for serial and mass production, especially of smaller parts and components

## Slide 329: Types of protrusions
The protrusions can be either natural or made by pressing or
machining; inserted protrusions are also used.
The shape and properties of the protrusions (stiffness and volume) have a significant effect on the welding process and the resulting weld quality.
The protrusions must not be deformed before they have melted.
Only then does the protrusion collapse and welding occurs.
Part of the molten and plastic material is extruded in the form of a protrusion, which is an accompanying phenomenon of a well-made weld.

## Slide 330: Principle of protrusion welding
In the initial phase of the welding process, the welding current is concentrated in places where the protrusions abut the second welded sheet.
The increased current density ensures a sharply limited local heating, and in a time corresponding approximately to the disappearance of the transient resistances, the heated protrusion collapses and the sheets abut each other.
In the further course of the welding process, the fusible lens grows in the joint, similarly to spot welding.
Protrusion (Stud) welding is used for sheets with thicknesses from 0.4 to 6 mm (exceptionally even more).

## Slide 331: Nature of protrusion welding
Welding parameters:
The basic quantities for protrusion welding are considered to be the same quantities as for spot welding.
Hard and soft welding modes can also be used.
However, when choosing parameters, it does not depend so much on the welded thicknesses, but on the floor plan of the weld surface

## Slide 332: Nature of protrusion welding
Types of created connections:
With the help of protrusion welding, it is possible to create:
interleaved joints
(in the case of embossed protrusions in the sheet, the weld resembles a multipoint joint),
butt joints
(created by massive protrusions, such as rods and tubes),
cross joints
(created by crossing wires or rods),
special joints
(created using embedded
protrusions between welded parts).

## Slide 333: Resistance CONTACT welding
We divide butt welding into two basic types:
compression welding
welding with fusion

## Slide 334: Contact stamping/Butt welding
Presses or special welding machines with a horizontal arrangement are used for this method.
Weld surfaces must be machined clean before welding so that the surfaces are parallel and perpendicular to the clamping axis.
No dirt must remain on the welded surfaces and the welded parts must rest on the entire contact surface with regard to ensuring the metallurgical quality of the weld.
The basic welding parameters are the same as for spot welding. Instead of the welding time, however, the so-called compaction length is set.
Large pressing forces are used, and a small protrusion is formed.
The material may not be fully melted in this method of welding
(this is actually a form of "blacksmith welding", where the material is welded in a plastic state) - pressure method.

## Slide 335: Contact stamping welding
During stamping welding, the material is heated by the welding current, which softens it.
It gradually melts and presses into itself until the limit switch switches off the welding current.
A protrusion is formed, which continues even after the welding current is switched off until the material solidifies.

## Slide 336: Butt/Contact welding with melting
In this method of welding, the welded parts are clamped in the same way as in butt welding, but without mutual contact of the two welded parts.
The electrical circuit is not closed. Only when the welded parts approach slightly (with little force) and immediately tear off, will local overheating to the melting temperature occur at some points of contact between the faces.
This movement is repeated in reverse and the melted area gradually increases to the entire cross-section, which is accompanied by sprays of oxides from the melt.
This process is called desoldering; the cycle lasts from a few seconds to tens of seconds.

## Slide 337: Butt/Contact welding with melting/desoldering
The welded surfaces are heated by the effects of electric arcs, which gradually arise in the places of random contacts of unmachined welded surfaces during their mutual approach under voltage.
Electric arcs gradually arise and disappear again; the weld surfaces are heated to the melting temperature and their melting takes place as the parts are continuously approached.
The so-called phase 1 – desoldering ends with continuous melt covering both faces of the welded parts.
However, phase 2 – compression immediately follows. During this phase, the molten parts are energetically pressed together and the current is switched off.

## Slide 338: Butt welding with melting/desoldering
Weld surface protection
is ensured during the welding process by overpressure of metal vapours; the compression phase must occur during desoldering after sufficient heating of the welded parts.
The basic welding parameters are:
welding current (current density),
desoldering rate,
melting time,
welding force (specific compaction pressure),
compression speed,
welding time.

## Slide 339: Use of butt resistance welding
Butt joints are formed.
in addition to full cross-sections, various hollow sections are also welded
(also corner welds of door frames, window frames, etc.).
It is possible to weld unalloyed, low-alloyed and high-alloyed steels and their mutual combinations as well as combinations with non-ferrous metals.
Butt/contact compression welding is used mainly for welding wires from diameters of 0.4 mm and bars of smaller diameters up to a cross-section of 600 mm2.
Mainly for processing wires, conductors, in welding concrete reinforcement, extending drills, connecting band saws, in the production of chains
Butt/Contact fusion welding can be used for cross-sections larger than 105 mm2 (normally cross-sections up to 3,000 mm2).
Wide application in the production of transport vehicles (e.g. wheel rims, car axle pins and joints are welded), rail welding, etc.

## Slide 340: Resistance welding equipment

## Slide 341
Thank you for your attention.

## Slide 342: Material weldability
expresses the suitability of the metal for welding. It characterizes the change of its properties in the thermally affected area due to the effect of the welding temperature cycle.
The suitability of the metal for welding is ensured, in particular, by
1) chemical composition (affects the behaviour of the weld bath; tendency to form turbid structures; tendency to ageing and susceptibility to cracking)
2) metallurgical method of material production, method of casting and forming (material purity, inclusions, grain size, microstructure, anisotropy of properties)
3) heat treatment

## Slide 343: Technological weldability
expresses the influence of the used welding type (method) and technology
on the properties of the welded joint.
It is ensured by the following basic factors:
welding method (heat input)
additive material
welding parameters
the procedure of laying the individual layers of the weld
thermal welding mode
heat treatment of the welded joint

## Slide 344: Structural weldability
expresses the influence of the design of the welded joint for the given operating conditions.
It is ensured by the following basic factors:
material thickness
shape, size, arrangement and number of joints
shape and preparation of welded surfaces
stiffness of the joint in the weldment
stress distribution depending on the stress and also the elimination of structural notches (sudden changes in stiffness, crossing of welds, too small fillet weld, etc.)

## Slide 345: Weldability must ensure:
Metallurgical functions
The base material combines with the weld metal without forming unwanted components and alloys.
Mechanical conditions
The joint must be free of defects (pores, cracks), slag, shrinkage and deformation.
Useful properties
The weld must perform its function under different operating conditions (extreme temperatures, corrosive environments, fatigue, high pressures, etc.).

## Slide 346: Weldability evaluation– standard ČSN 05 1309
Original standard valid until 1991
level 1a)
weldability guaranteed - the material manufacturer guarantees weldability (up to 0ºC) without special welding measures
level 1b)
weldability guaranteed but conditional - the manufacturer guarantees the weldability of the steel in compliance with the specified conditions (e.g. preheating before welding)
level 2)
weldability good - the manufacturer does not guarantee weldability, but these steels give, in most cases, satisfactory welded joints
level 3)
difficult to weld - for these materials, it is usually not possible to achieve a satisfactory quality of the welded joint (even if special measures are observed)
these materials are not recommended for welding

## Slide 347: Weldability evaluation
The suitability of the material for welding under certain technological or constructional conditions or technological conditions of welding of a certain material to achieve a functionally suitable joint.
Data on the suitability of metals for welding are given in the material’s data sheets.
Weldability as a complex characteristic has been evaluated since 1991 according to the updated standard ČSN 05 1309.
Today, this assessment is based on two groups of indicators:
indicators of the integrity of welded joints - characterize the resistance to cracking and other unacceptable defects
indicators of mechanical properties of welded joints - characterize the changes of individual properties in the area of the joint as a result of welding

## Slide 348: Weldability evaluation
Indicators of mechanical properties of welded joints:
tensile strength of the welded joint (tested according to ČSN 05 1121)
hardness of the welded joint (ČSN EN 1043-1,2)
notched toughness (impact work) of the heat-affected zone (TOO) of the welded joint (ČSN 05 1125)
Indicators of weld integrity:
resistance to cold cracking (tested according to standard ČSN 05 1142)
resistance to hot cracking (ČSN 05 1143)
resistance to annealing cracking (ČSN 05 1144)
resistance to lamellar cracking (ČSN 051314)

## Slide 349: Welding procedure qualification
- ČSN EN ISO 15 6XX
Welding procedure test
pWPS – Preliminary Welding Procedure Specification
WPS – Welding Procedure Specification
WPQR – Welding Procedure Qualification Record

## Slide 350: Welding procedure qualification
- ČSN EN ISO 15 6XX
Welding procedure test ČSN EN ISO 15 614
- is the production and testing of a standardized test piece specified in the pWPS and performed for the purpose of qualification of the welding procedure (documented by the WPQR protocol).
Pre-production welding test ČSN EN ISO 15 613
- is a welding test that has the function (level) of a welding procedure test, but is based on a non-standardized test piece that is typical of the production conditions. (Suitability for mass production). It is documented by the WPQR protocol.

## Slide 351: Welding procedure qualification
- ČSN EN ISO 15 6XX

## Slide 352: Welding procedure qualification
- ČSN EN ISO 15 6XX
Standardized welding procedure ČSN EN ISO 15 612
is a welding process specification that has been qualified by a welding process test that applies to many manufacturers for wider use of the qualified procedure. It is documented by the WPQR protocol. The welding equipment must allow for checking (indication) of all basic welding parameters.
Previous welding experience ČSN EN ISO 15 611
is a document on documented tests that demonstrate that the welding procedures used by the manufacturer in production were capable of performing welds of acceptable (required) quality over a period of time. It is documented by the WPQR protocol.
Tested welding material ČSN EN ISO 15 610
is a welding material or combination of welding materials tested in accordance with the relevant standards for testing welding material supplied in accordance with Technical Delivery Regulations and Conditions (TDP). It is documented by the WPQR protocol.

## Slide 353: WPS
Welding Procedure Specification
ČSN EN ISO 15 609
Determination and qualification of welding procedures for metallic materials - Determination of welding procedure
Part 1: Arc welding for
all welds
Part 2: Flame welding