# HEAT TREATMENT AND SINTERING

### ESF II project of the University of West Bohemia in Pilsen, reg. number: CZ.02.2.69/0.0/0.0/18_056/0013239

## Laboratory task 4: Cementation according to specified parameters

### Name and Surname:

- Mark the received samples and clean them properly/meticulously.

- Carry out powder cementation on the specified material (C15, 15NiCr13, 16MnCr5).  Cement at the assigned temperature (890°C, 910°C, 930°C). Cementation period 4 hours (plus heating time 1.5 hours).

- Select a suitable hardening temperature, hardening environment and perform hardening. Justify everything.

- Evaluate the relevant layer and core – metallographically, by measuring microhardness.

- Graph the results; describe the microstructure.

  - Schematically draw the microstructure of the layer and the core in a box measuring 50mm x 50mm

- Discuss the results using your colleagues' results!

  - Compare layer thicknesses, core strengths, etc.