EVALUATION OF SURFACE TREATMENTS

- ORGANIC COATINGS

powder plastic paints and coatings

- 70% of surface treatments in mechanical engineering

Substrate protection 	- barrier function of the coating

- ability of the coating not to let the

active components of the environment aggressively penetrate

- surface blocking

- the ability to prevent the occurrence of corrosion processes due to the physical and chemical bonds of the substrate with the coating

Formation of degradation	 caused by:

- penetration of the corrosive environment through the coating system

-  disruption of the coating

- impairing the adhesion between the base material and coating

Degradation	caused by:

dusting, chalking, blistering, swelling, cracking, undercorrosion, loss of adhesion, etc.

2. INORGANIC NON-METAL COATINGS

conversion coatings, enamels, thermal sprays, silicate coating, carbide-based coatings, silicides, borides, cermets, etc.

Protection mechanism 	- barrier effect

- blocking of the surface

Degradation	- damaged integrity under increased stress

- loss of adhesion

- loss of gloss

3. METAL COATINGS

20% 		total production of surface treatments

12% 		generated electrochemically (galvanically)

5% 		by immersion in molten metal

3% 		by thermal spraying

0.5% 	by physical methods

Mechanism of protection

- immunity - thermodynamic improbability of corrosion

- passivity - formation of thin, compact layers on the surface

- protective layer of corroding products

Major causes of degradation

- damage to the integrity of the protective coating

- local damage of passivity

- disruption of the protective layer

- exposure of the substrate (loss of adhesion)

- corrosion of the base material

4. COMBINED COATINGS

The most common combinations (double and multilayer coatings):

- heat-formed metal coating + paint

- heat-formed metal coating + powder plastic

- heat-formed metal coating + silicate coating

- organic coating + vacuum-steamed + organic coating

Mechanism of protection

- depends on the type of combination

Manifestations of degradation

- 	depends on the nature of the loss of protective and functional properties of individual coatings

INPUT INSPECTION OF MATERIAL, RAW MATERIALS AND BATHS

Input inspection 	- verification of material and raw material properties

for creating coating systems

(paints, powders, frits, etc.)

or for the preparation of baths (chemicals, etc.)

- or basic properties of newly deployed baths

Viscosity	-  inner friction of fluids

- resistance of fluid to tangential stress

at laminar flow:

- liquid particles adjacent to walls do not move

- the velocity of particles increases towards the axis of the tube

- tangential stress τ [MPa] created by internal friction at the contact surface of two layers of different velocities v:

τ = η

- speed gradient

η	- viscosity (dynamic) -  internal friction coefficient (dynamic) [Pa.s]

υ =

υ 	- kinematic viscosity -  kinematic coefficient of internal friction [m2 s-1]

ρ	- density [kg.m-3] 		ρ =

Determination of viscosity according to Hőppler

Hőppler viscometer 	test tube inclined at an angle of 10 ° to the vertical axis in a tempering jacket

Tempering: 	measurement of the time of passage of the ball between two marked places on the inclined tube

M - measuring tube

A - screw head

B - metal plate

C - vent insert

t1	- supply tube

for tempering liquid

t2	- drain pipe

for tempering liquid

T - thermometer

L - spirit level

Determination of viscosity according to Hőppler

Working procedure:

- Close the measuring tube at the bottom with a stopper and a screw cap

- Fill the tube with liquid to about 2.5 cm below the edge

- Using tweezers, insert the ball

- Insert the vent insert and close the tube with a tight cap

- Place the viscometer stand in a horizontal position

- Using rubber hoses, connect the tempering jacket of the viscometer to the thermostat

- Set the temperature, turn on the pump and heating

- Turn the viscometer and measure the passage time of the ball

- After the measurement, unscrew the bottom cap and release the ball into the catcher

Calculation of dynamic viscosity:

η = K (ρk - ρt) . t

η – dynamic viscosity

K – device constant

ρk – density of the test ball

ρt – density of the test liquid

t – average time of ball fall

Bubble viscometer

Principle: comparing the passage of the bubble in the sample with substances of known viscosity

Consistency 	- depends on viscosity, characterizes fluidity,

and thus the workability of the paint

Orientation determination - perfect mixing of the sample with a spatula, length about 250 mm, width 25 mm

- the spatula is removed from the container and tilted at an angle of about 60°

Consistency is expressed in the following degrees:

- very little viscous – very thin (e.g. water)

- slightly viscous – thin (e.g. pure oil)

- medium viscous – medium (e.g. glycerine)

- highly viscous – very thick (e.g. gear oil)

Outflow time measurement

- simple, fast-operating, even laboratory method

Consistency determined by the outflow time of a given volume from a standard cup (outflow diameter 4 mm) at a temperature of 20oC

Workflow

- the outlet of the cup fixed in the stand is closed

- the paint is poured over the rim into the cup

- excess material is removed with a glass plate

- the measurement determines the time from the release of the nozzle to the moment of the first rupture of the continuous stream of outflowing paint

| Application | Outflow time [s] |
| --- | --- |
| Brush, glove | 50-80 |
| Pneumatic spraying | 20-35 |
| Hot spraying | 70-100 |
| Soaking, watering | 20-40 |

Determination of viscosity: it is read from a table or graph

Sedimentation

- difficulty in mixing the pigment sediment

- the force required for the test tool to penetrate the deposit to the bottom of the container in which the paint is stored

ASTM method     - handling of a spatula weighing 45 g with a 21 mm wide and 121 mm long metal plate is evaluated

Pigment deposit:

- easy to mix

- miscible

- difficult to mix

- immiscible

Density (specific gravity)

ρ =   	[kg.m-3]

Relative density  - a dimensionless number indicating the ratio of the weight of a certain volume of, e.g., paint to the weight of the same volume of water at a specified temperature

Determination of density by immersion densitometer

Densitometer

- sealed glass tube calibrated to a certain temperature

- floats in a liquid in a vertical position

- then immerses deep until the weight of the expelled liquid is equal to the weight of the densitometer (Archimedes' law)

- the depth of immersion depends on the density of the liquid

- the density value is read on the scale of the densitometer

Disadvantages of the method:

- the need for a larger sample

- small measuring range

- cannot be used for measuring pigmented paints

and high-viscosity varnishes

Determination of density by pycnometer

Principle:	the known volume of the test sample is weighed

Water value of the pycnometer (measuring container):

O = (b – a) / 0,99823

a - weight of empty pycnometer,

b - weight of the pycnometer filled with water

0.99823 [kg.m-3] – density of water at 20°C

Sample density:

ρv =  (c – a) / O

c - weight of the pycnometer with the sample

Determination of density with a metal cup

More suitable for paints: determination of weight in a metal cup containing 100 ml

- the volume of the test vessel is determined with distilled water

- after tempering the container and the sample, the container is filled

- after a further 30 minutes of tempering, the excess sample is removed by pressing the lid

Density  ρ20  [kg. l-1]:

ρ20 = (G3 – G1) / V

G3 - empty container weight [g]

G1 - filled container weight [g]

V  - container volume [ml]

Content of non-volatile components

Non-volatile components (dry matter) 	- a summary of film-forming and solid substances

after evaporation of solvents and thinners they remain as a protective layer on the surface

the content of non-volatile components – affects

- the course of coating formation

- thickness and protective properties

expression: weight in %

The essence of measuring methods	- determination of the residual amount of paint after heating the sample under the prescribed conditions

According to the  ČSN 67 3031standard:

- asphalt, oil, synthetic NH 			2 hours at 135°C

- synthetic firing NH				3 hours at 135°C

- nitrocellulose, polymeric NH		4 hours at 80°C

Determination of non-volatile components in drying oven

Sample of paint in a petri dish

- weighed on an analytical balance

- heated at the prescribed temperature and time in the drying oven

Non-volatile matter content: ratio of the weight of the sample after drying to the weight of the original sample

In operation 	instead of a petri dish, lids made of tin coated with paint are used

Determination of dry matter in %:

S =  .100 %

a – lid weight [g]

b - weight of the lid with a sample of paint [g]

c - weight of the lid after drying [g]

Dilutability

Ability of the paint to be diluted with the appropriate thinner while maintaining the required technical properties of the paint and the required paint quality

In practice: simple empirical methods (based on experience)

Qualitative test

Suitability of the respective diluent

Glass beaker:

- 50 g sample of paint

- intensive mixing

- addition of diluent to a weight ratio of 1: 1, possibly. 1: 2

there must be no clouding (varnishes), villi or precipitation of the binder

Maximum diluent addition test

- until the formation of permanent turbidity of paints

- until the formation of precipitates in pigmented paints

Test to determine the amount of diluent for a given consistency

- weighing 120 ml of the paint sample

- adding 5 weight% diluent

- mixing

- determination of consistency with a spout cup

- repeating with a new sample of paint and adding more diluent

- creating a course of dependence of the change in consistency on the amount of the diluent

Flash point of paints

Flash point – the lowest temperature [°C] at which a substance heated under defined conditions generates so many vapours that their mixture with air ignites when the initiating flame approaches, and immediately goes out

Burning mixtures with a flash point lower than room temperature T

According to the value of the flash point - classification of NH into a safety class

- important for transport, storage and processing of NH

I.  - flammable liquids with a flash point up to 21°C (alcohol, petrol, etc.)

II. - flammable liquids with a flash point from 21°C to 65°C (diesel, kerosene, etc.)

III. - flammable liquids with a flash point between 55°C and 100°C

IV. - liquids with a flash point above 100°C

Liquids up to a flash point of 250°C are considered flammable

Pensky-Martens device

with integrated fire extinguisher

Combustion temperature – the lowest temperature at which a substance heated under defined conditions generates so many vapours that their mixture with air ignites when the initiating flame approaches.

Ignition temperature – the lowest temperature at which a mixture of vapours or gases of a given substance with air ignites under prescribed conditions (only by the action of heat)

pH value (acidity number)

- negative decimal logarithm of hydrogen ion activity

- to determine the acidity or alkalinity of baths

- is checked		 during the preparation of baths

during technological processes

(chemical and electrochemical processes)

for waste products, etc.

Potentiometric measurement 	measurement of the potential of a cell formed by a measuring glass and comparative calomel electrode in the measured environment

For evaluation of paint substance pH, the

acidity number								is used:

the amount of KOH needed to neutralize the free components in 1 g of sample

high acidity number – effect:

- on the corrosion of the substrate under the paint

- for film ageing and storage

For varnishes:  determination by titration (volumetric analysis)

- titration flask

- weight: 10 to 50 g of paint

- dissolves with a neutral mixture of benzene and ethanol (2:1)

- the sample can be heated for better dissolution

- cooling

- KOH is titrated (dripped) until a pink colour appears (phenophthalein)

- end of titration - colour does not change within 30 s

Calculation of acidity number:

A.n. = a . f . 5,611 / b

a – KOH consumption [ml]

f – KOH factor

b – sample weight [g]